Crystal Structure Report for Kovacs

Submitted by Elaine Nam

Sample ID – 430nm

by Jason Benedict

X-ray Crystallography Laboratory

University of Washington

28. August 2006
Data backup accessibly through http:

URL: 
http://cad4.cpac.washington.edu/structures/kovacs/elaine/430nm

Username: 
xray-user

Password: 
hkl-data

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210 

Email: kaminsky@wintensor.com
Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures. Even I  have to pay for my own structures for my research.

A green crystal prism cut down to 0.048 x 0.24 x 0.24 mm was mounted on a glass capillary with oil.  Data was collected at -143oC with two sets of exposure as follows:

Scan 

Type
Scanlength (deg.)  start (deg.)
(     
(
(     
( 

1
      
(        
133.6




3.70
97.7
160  
 0 

2
      
(        
86.5




3.70
-145.9
-200.1 
 74.1           

Crystal-to-detector distance was 30 mm and exposure time was 30 seconds per degree for all sets.  The scan width was 2.0o.   Data collection was 94.9% complete to 28.38o and 97.5% complete to 25o  in (.  A total of  218974 partial and complete reflections were collected covering the indices, h = -17 to 17, k = -11 to 11,  l = -21 to 21. 2427 reflections were symmetry independent and the Rint = 0.0437 indicated that the data was of better than average quality (0.07). 

Indexing and unit cell refinement indicated a orthorhombic P lattice.  The space group was found to be P n m a (No.62). 

The data was integrated and scaled using hkl-SCALEPACK. This program applies a multiplicative correction factor (S) to the observed intensities (I) and has the following form:


[image: image1.wmf]22

2(sin)/

S = ()/scale

B

e

ql

-


S is calculated from the scale and the B factor determined for each frame and is then applied to I to give the corrected intensity (Icorr).

Solution by direct methods (SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. 

All hydrogen atoms were located using a riding model. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares. 

Both the metal complex and counter ion reside on a mirror plane, thus the asymmetric unit contains only half the atoms of the full molecules. The full metal complex is illustrated on the following page. The PF6- anion is heavily disordered, as well as C6. Attempts were made to split C8, an atom with a large Ueq, however, the resulting models did not lower the R value nor did they possess sensible unrestrained bond lengths.




_1097643391.unknown

