Crystal Structure Report for Mayer

Submitted by Adam Wu 

Sample ID – AW03

by Dawn Cohen and Jason Benedict

X-ray Crystallography Laboratory

University of Washington

22. March 2005
Data backup accessibly through ftp:

computer: 

chmraypc.cpac.washington.edu

login: 

anonymous

password:

(your name or email address)

location: 
c:\structures\mayer\adamwu\AW03

Data backup accessibly through http:

URL: 
http://cad4.cpac.washington.edu/structures
Username: 
xray-user

Password: 
hkl-data

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210 

Email: kaminsky@wintensor.com
Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures. Even I  have to pay for my own structures for my research.

A red crystal prism cut down to 0.12 x 0.12 x 0.1 mm was mounted on a glass capillary with oil.  Data was collected at -143oC with two sets of exposure as follows:

Scan 

Type
Scanlength (deg.)  start (deg.)
(     
(
(     
( 

1
      
(        
136.6




3.70
-152.3
160  
 0 

2
      
(        
96.5




0
-25.9
-191.5 
 74.1           

Crystal-to-detector distance was 30 mm and exposure time was 30 seconds per degree for all sets.  The scan width was 1.2o.   Data collection was 90.3% complete to 24.7o   in (.  A total of  42213 partial and complete reflections were collected covering the indices, h = -13 to 13, k = -16 to 18,  l = -14 to 14.  3666 reflections were symmetry independent and the Rint = 0.1936 indicated that the data was of  less than average quality (0.07). 

Indexing and unit cell refinement indicated a monoclinic P lattice.  The space group was found to be P 21/c (No.14). 

The data was integrated and scaled using hkl-SCALEPACK. This program applies a multiplicative correction factor (S) to the observed intensities (I) and has the following form:

S = exp(2B(sinq/()2)/ scale

S is calculated from the scale and the B factor is determined for each frame and is then applied to I to give the corrected intensity (Icorr).

Solution by direct methods (SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. 

All hydrogen atoms were located using a riding model. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares. 

Counter ions present indicated that Ru is in the 3+ charge state. Distances between those atoms coordinating to Ru are consistent with those of another structure (AW02) containing Ru 3+. Poor sample quality caused the collection of a poor quality data set and therefore the identity of the water molecule is not absolute. While the data set is useful for determining the byproducts of the reaction, the structure is unfortunately unpublishable.




