Crystal Structure Report for Jim Mayer
Submitted by Adam Wu 

Sample ID – AW11
by Werner Kaminsky

X-ray Crystallography Laboratory

University of Washington

29. June 2006
Data backup accessibly through http:

URL: 
http://cad4.cpac.washington.edu/structures
Username: 
xray-user

Password: 
hkl-data

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210 

Email: kaminsky@wintensor.com
Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures. Even I  have to pay for my own structures for my research.

A black prism, size 0.23 x 0.10 x 0.08 mm was mounted on a glass capillary with oil.  Data was collected at -143oC with two sets of exposure as follows:

Scan 

Type
Scanlength (deg.)  start (deg.)
(     
(
(     
( 

1
      
(        
182.0




3.70
-184.5
160  
 0 

2
      
(        
31.5




3.70
-145.9
-165.1 
 74.1           

Crystal-to-detector distance was 30 mm and exposure time was 90 seconds per degree for all sets.  The scan width was 2o.   Data collection was 94.9% complete to 28.31o and 98.3% complete to 25o  in (.  A total of  65546 partial and complete reflections were collected covering the indices, h = -13 to 13, k = -23 to 25,  l = -31 to 31.  10787 reflections were symmetry independent and the Rint = 0.1274 indicated that the data was of slightly less than average quality (0.07). 

Indexing and unit cell refinement indicated a monoclinic P lattice.  The space group was found to be P 21/c (no. 14). 

The data was integrated and scaled using hkl-SCALEPACK. This program applies a multiplicative correction factor (S) to the observed intensities (I) and has the following form:


[image: image1.wmf]22

2(sin)/

S = ()/scale

B

e

ql

-


S is calculated from the scale and the B factor determined for each frame and is then applied to I to give the corrected intensity (Icorr).

Solution by direct methods (SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. 

All hydrogen atoms were located using a riding model. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares. 

Two independent molecules occupy the assymmetric unit of the structure. In total there are 8 molecules in the monoclinic unit cell. The fluorines show the expected strong thermal motion, triggering a warning by cifcheck. The following response was added to the cif to explain this as an intrinsic feature of the structure:

 # start Validation Reply Form 

_vrf_PLAT242_shelxl 

; 

RESPONSE: Fluorinated methyl groups C6, C10, C23, C24, C28 

show strong librative motion which translates through to 

neighbouring ligands C5, C18, C21, C22, C35, C36.

; 

# end Validation Reply Form



_1097643391.unknown

