Crystal Structure Report for Kovacs
Submitted by Lisa Brines 

Sample ID – brines14_2
by John Freudenthal
and Werner Kaminsky
X-ray Crystallography Laboratory

University of Washington

19. December 2006
Data backup accessibly through http:

URL: 
http://cad4.cpac.washington.edu/structures/goldberg/andy/avpiv82
Username: 
xray-user

Password: 
hkl-data

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210 

Email: kaminsky@wintensor.com
Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures. Even I  have to pay for my own structures for my research.

A clear yellow crystal needle cut down to 2 x 0.1 x 0.1 mm was mounted on a glass capillary with oil.  Data was collected at -143oC with one set of exposure as follows:

Scan 

Type
Scanlength (deg.)  start (deg.)
(     
(
(     
( 

1
      
(        
181.0




3.70
-169
160  
0
2

(
106.5




3.70
-145
-200
74      

3

(
31.6




3.70
145
118
-74      

Crystal-to-detector distance was 30 mm and exposure time was 60 seconds per degree for all sets.  The scan width was 3.0o.   Data collection was 88.6% complete to 15.0o in (.  A total of  39561 partial and complete reflections were collected covering the indices, h = -14 to 14, k = -7 to 7,  l = -20 to 20.  2315  reflections were symmetry independent and the Rint = 0.1073 indicated that the data was of less than average quality (0.07). 

Indexing and unit cell refinement indicated a orthorhombic P lattice.  The space group was found to be Pbcn (No.60). 

The data was integrated and scaled using hkl-SCALEPACK. This program applies a multiplicative correction factor (S) to the observed intensities (I) and has the following form:

S = exp(2B(sinq/()2)/ scale

S is calculated from the scale and the B factor is determined for each frame and is then applied to I to give the corrected intensity (Icorr).

Solution by direct methods (SHELXS97) produced a partially complete heavy atom phasing model consistent with the proposed structure. 

All hydrogen atoms were located using a riding model. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares. 

The molecule appears to be an iron dimer complex. The solvent CH2Cl2 occupies only partially the shown position. The charge is balanced by chlorides. The quality of the crystal was problematic, thus the data does not reach sufficient completeness at larger scattering angles. As a result, thermal parameters are not well defined and had to be restrained. Although edited for publication, a possible publication may benefit from a better sample.



