Crystal Structure Report for Julie Kovacs

by M. Coggins and W. Kaminsky

Sample Submitted by Ben Leipzig 

ID – Ben30

X-ray Crystallography Laboratory

University of Washington

16. January 2013
Data backup accessibly through http:

URL: 
http://cad4.cpac.washington.edu/structures
Username: 
xray-user

Password: 
hkl-data

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210 

Email: kaminsky@chem.washington.edu
Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures. Even I  have to pay for my own structures for my research.

A purple, twinned prism, measuring 0.4 x 0.1 x 0.05 mm3 was mounted on a loop with oil.  Data was collected at -173oC on a Bruker APEX II single crystal X-ray diffractometer, Mo-radiation. Crystal-to-detector distance was 40 mm and exposure time was 10 seconds per degree for all sets.  The scan width was 0.5o.   Data collection was 96.1% complete to 25o in (.  The sample showed concave interceptions on its edges which are typical signs of twinning. 
The raw data appeared indeed twinned. With CELL_NOW
 a 180o twin operation about  (1 0 0 )  was found which, if unresolved, would cause considerable overlap of diffraction peak intensities from different domains of the sample. Multi-domain integration with SAINT within the APEX2 software package by Bruker
 and absorption correction with twinabs
 removed the overlap. A total of 39546 reflections were collected with 4041 symmetry independent reflections covering the indices, h = 0 to 19, k = -11 to 0,  l = -17 to 17 (after merging for HKLF 5 file format)  with Rint = 0.1379 indicated that the twin-refined data was reasonable (average quality 0.07). Indexing and unit cell refinement indicated then a primitive monoclinic lattice.  The space group was found to be P 21/c  (No.14). 
Solution by direct methods (SHELXS, SIR97
) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL97.
,
 Scattering factors are from Waasmair and Kirfel
. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C(H distances in the range 0.95(1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares
The structure is of high quality and ready for publication. Table 1 summarizes the data collection details. 

[image: image1.png]



Figure 1. ORTEP
 of the asymmetric unit with thermal ellipsoids at the 50% probability. 
Table 1: Crystallographic data for the structures provided.

Empirical formula 
C24 H36 B2 Cu F8 N4 S2

Formula weight 
681.85

Temperature 
100(2) K

Wavelength 
0.71073 Å

Crystal system 
Monoclinic

Space group 
P 21/c

Unit cell dimensions
a = 13.869(3) Å
= 90°.


b = 8.7639(14) Å
= 103.101(12)°.


c = 12.427(2) Å
 = 90°.

Volume
1471.2(5) Å3
Z
2

Density (calculated)
1.539 Mg/m3
Absorption coefficient
0.958 mm-1
F(000)
702

Crystal size
0.40 x 0.10 x 0.05 mm3
Theta range for data collection
2.87 to 30.14°.

Index ranges
0<=h<=19, -11<=k<=0, -17<=l<=17

Reflections collected
39546

Independent reflections
4041 [R(int) = 0.1379]

Completeness to theta = 25.00°
96.1 % 

Max. and min. transmission
0.9537 and 0.7006

Refinement method
Full-matrix least-squares on F2
Data / restraints / parameters
4041 / 0 / 189

Goodness-of-fit on F2
1.041

Final R indices [I>2sigma(I)]
R1 = 0.0975, wR2 = 0.2221

R indices (all data)
R1 = 0.1831, wR2 = 0.2657

Largest diff. peak and hole
1.944 and -1.113 e.Å-3
� Sheldrick, G. M. (2005). CELL_NOW. University of Goettingen, Germany.


� Bruker (2007) APEX2 (Version 2.1-4), SAINT (version 7.34A), SADABS


(version 2007/4), BrukerAXS Inc, Madison, Wisconsin, USA.


� Sheldrick, G. M. (2007). TWINABS. University of Goettingen, Germany.


� (a) Altomare, A.; Burla, C.; Camalli M.; Cascarano L.; Giacovazzo C.; Guagliardi A.;   Moliterni A.G.G.; Polidori G.; Spagna R. J. Appl. Cryst. 1999, 32, 115-119; (b) Altomare, A., Cascarano, G., Giacovazzo, C., Guagliardi, A., J. Appl. Cryst. 1993, 26, 343.


� Sheldrick, G. M. SHELXL-97: Program for the Refinement of Crystal Structures 1997 University of Gottingen, Germany.


� Mackay, S.; Edwards, C.; Henderson, A.; Gilmore, C.; Stewart, N.; Shankland, K.; Donald, A.; MaXus: a computer program for the solution and refinement of crystal structures from diffraction data. University of Glasgow, Scotland, 1997.


� Waasmaier, D.; Kirfel, A. Acta Crystallogr. A. 1995, 51, 416.


� Farrugia, L. J. Appl. Cryst. 1997, 30, 565





