Crystal Structure Report for A. Vignesh
by Werner Kaminsky

ID – CoApMBH
X-ray Crystallography Laboratory

University of Washington

07. June 2018
Data Collection  started: 3/18/2018
Documentation finished: 6/7/2018
Data backup accessibly through http:

URL: http://cad4.cpac.washington.edu/structures
W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210 

Email: kaminsky@chem.washington.edu
Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures. 

An orange prism, measuring 0.60 x 0.04 x 0.01 mm3 was mounted on a loop with oil.  Data was collected at -173oC on a Bruker APEX II single crystal X-ray diffractometer, Mo-radiation.
Crystal-to-detector distance was 41 mm and exposure time was 30 seconds per frame for all sets.  The scan width was 0.5o.   Data collection was 99.4% complete to 25o  in (.  A total of  12177 merged reflections were collected covering the indices, -10<=h<=10, -25<=k<=25, -44<=l<=44.  6456 reflections were symmetry independent and the Rint = 0.0774 indicated that the data was of average quality.  Indexing and unit cell refinement indicated a primitive orthorhombic lattice.  The space group was found to be P b c n  (No. 60). 

The data was integrated and scaled using SAINT, SADABS within the APEX2 software package by Bruker.
 

The contribution of disordered solvent to the diffraction pattern was removed with SQUEEZE

Solution by direct methods (SHELXS, SIR97
) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL97.
,
 Scattering factors are from Waasmair and Kirfel
. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C---H distances in the range 0.95-1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares.
The structure is of high quality and ready for publication. Table 1 summarizes the data collection details. Figure 1 shows an ORTEP
 of the asymmetric unit.
[image: image1.jpg]



Figure 1. ORTEP of the structure with thermal ellipsoids at the 50% probability level. Disorder solvent SQUEEZED.

Table 1: Crystallographic data for the structures provided.

Empirical formula 
C30 H28 Co N6 O4

Formula weight 
595.51

Temperature 
100(2) K

Wavelength 
0.71073 Å

Crystal system 
Orthorhombic

Space group 
P b c n

Unit cell dimensions
a = 8.7585(7) Å
= 90°.


b = 20.2282(14) Å
= 90°.


c = 35.669(2) Å
 = 90°.

Volume
6319.4(8) Å3
Z
8

Density (calculated)
1.252 Mg/m3
Absorption coefficient
0.585 mm-1
F(000)
2472

Crystal size
0.600 x 0.040 x 0.010 mm3
Theta range for data collection
2.014 to 26.416°.

Index ranges
-10<=h<=10, -25<=k<=25, -44<=l<=44

Reflections collected
12177

Independent reflections
6456 [R(int) = 0.0774]

Completeness to theta = 25.000°
99.4 % 

Refinement method
Full-matrix least-squares on F2
Data / restraints / parameters
6456 / 0 / 374

Goodness-of-fit on F2
1.003

Final R indices [I>2sigma(I)]
R1 = 0.0474, wR2 = 0.1012

R indices (all data)
R1 = 0.1084, wR2 = 0.1217

Largest diff. peak and hole
0.436 and -0.567 e.Å-3
� Bruker (2007) APEX2 (Version 2.1-4), SAINT (version 7.34A), SADABS (version 2007/4), BrukerAXS Inc, Madison, Wisconsin, USA.


� (a) A. Spek, J. Appl. Cryst. (2003), 36, 7-13; 


   (b) P. van der Sluis & A. L. Spek, Acta Cryst. (1990). A46, 194-201.


   (c) Spek, A. L. (2009). Acta. Cryst. D65, 148-155.


� (a) Altomare A, Burla C, Camalli M, Cascarano G L, Giacovazzo C, Guagliardi A,   Moliterni AGG, Polidori G, Spagna R. (1999) SIR97: a new tool for crystal structure determination and refinement Journal of Applied Crystallography, 32, 115-119. 


   (b) Altomare A, Cascarano G L, Giacovazzo C, Guagliardi A. (1993) Completion and refinement of crystal structures with SIR 92. Journal of Applied Crystallography, 26, 343-350.


� (a) Sheldrick GM. (1997) SHELXL-97, Program for the Refinement of Crystal Structures. University of Göttingen, Germany.


   (b) Sheldrick GM. (2013) Crystal structure refinement with SHELXL. Acta Cryst. (2015). C71, 3-8.


� Mackay, S.; Edwards, C.; Henderson, A.; Gilmore, C.; Stewart, N.; Shankland, K.; Donald, A. (1997) MaXus: a computer program for the solution and refinement of crystal structures from diffraction data. University of Glasgow, Scotland,.


� Waasmaier, D.; Kirfel, A. (1995) New Analytical Scattering Factor Functions for Free Atoms and Ions. Acta Crystallographica A., 51, 416-430.


� Farrugia LJ. (1997) Ortep-3 for Windows. Journal of Applied Crystallography, 30, 565





