Crystal Structure Report for 
A. Vignesh
by Werner Kaminsky

ID – CoApTH
X-ray Crystallography Laboratory

University of Washington

14. June 2018
Data Collection  started: 6/13/2018
Documentation finished: 6/14/2018
Data backup accessibly through http:

URL: http://cad4.cpac.washington.edu/structures
W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210 

Email: kaminsky@chem.washington.edu
Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures. Even I  have to pay for my own structures for my research.

A flat elongated orange prism, measuring 0.60 x 0.20 x 0.03 mm3 was mounted on a loop with oil.  Data was collected at -143oC on a Nonius Kappa CCD FR590 single crystal X-ray diffractometer, Mo-radiation.
Crystal-to-detector distance was 30 mm and exposure time was 60 seconds per degree for all sets.  The scan width was 2o.   Data collection was 99.7% complete to 25o  in (.  A total of  7043 merged reflections were collected covering the indices, -13<=h<=13, -17<=k<=18, -15<=l<=14.  3778 reflections were symmetry independent and the Rint = 0.0742 indicated that the data was of average quality (0.07).  Indexing and unit cell refinement indicated a primitive monoclinic lattice.  The space group was found to be P 2/c  (No.13). 

The data was integrated and scaled using hkl-SCALEPACK.
 This program applies a multiplicative correction factor (S) to the observed intensities (I) and has the following form:


[image: image1.wmf]22

2(sin)/

S = ()/scale

B

e

ql

-


S is calculated from the scale and the B factor determined for each frame and is then applied to I to give the corrected intensity (Icorr).

Solution by direct methods (SHELXS, SIR97
) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL97.
,
 Scattering factors are from Waasmair and Kirfel
. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C---H distances in the range 0.95-1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares.
The contribution of disordered solvent to the diffraction pattern was removed with SQUEEZE

The structure is of high quality and ready for publication. Table 1 summarizes the data collection details. Figure 1 shows an ORTEP
 of the asymmetric unit.
[image: image2.jpg]



Figure 1. ORTEP of the structure with thermal ellipsoids at the 50% probability level. Solvent SQUEEZEd.
Table 1: Crystallographic data for the structures provided.

Empirical formula 
C24 H20 Co N6 O2 S2

Formula weight 
547.51

Temperature 
130(2) K

Wavelength 
0.71073 Å

Crystal system 
Monoclinic

Space group 
P 2/c

Unit cell dimensions
a = 9.9855(13) Å
= 90°.


b = 13.8983(19) Å
= 104.224(7)°.


c = 11.4032(14) Å
 = 90°.

Volume
1534.0(3) Å3
Z
2

Density (calculated)
1.185 Mg/m3
Absorption coefficient
0.723 mm-1
F(000)
562

Crystal size
0.600 x 0.200 x 0.030 mm3
Theta range for data collection
2.840 to 28.299°.

Index ranges
-13<=h<=13, -17<=k<=18, -15<=l<=14

Reflections collected
7043

Independent reflections
3778 [R(int) = 0.0742]

Completeness to theta = 25.000°
99.7 % 

Refinement method
Full-matrix least-squares on F2
Data / restraints / parameters
3778 / 10 / 175

Goodness-of-fit on F2
0.943

Final R indices [I>2sigma(I)]
R1 = 0.0542, wR2 = 0.1247

R indices (all data)
R1 = 0.1000, wR2 = 0.1385

Largest diff. peak and hole
0.568 and -0.472 e.Å-3
� Otwinowsky, Z.; Minor, W. In: Methods in Enzymology; Carter, C. W., Jr., Sweet, R. M., Eds.; Academic Press: New York, 1997, 276, 307-326.


� (a) Altomare, A.; Burla, C.; Camalli M.; Cascarano L.; Giacovazzo C.; Guagliardi A.;   Moliterni A.G.G.; Polidori G.; Spagna R. J. Appl. Cryst. 1999, 32, 115-119; (b) Altomare, A., Cascarano, G., Giacovazzo, C., Guagliardi, A., J. Appl. Cryst. 1993, 26, 343.


� Sheldrick, G. M. SHELXL-97: Program for the Refinement of Crystal Structures 1997 University of Gottingen, Germany.


� Mackay, S.; Edwards, C.; Henderson, A.; Gilmore, C.; Stewart, N.; Shankland, K.; Donald, A.; MaXus: a computer program for the solution and refinement of crystal structures from diffraction data. University of Glasgow, Scotland, 1997.


� Waasmaier, D.; Kirfel, A. Acta Crystallogr. A. 1995, 51, 416.


� A. Spek, J. Appl. Cryst. (2003), 36, 7-13; P. van der Sluis & A. L. Spek, Acta Cryst. (1990). A46, 194-201.


� Farrugia, L. J. Appl. Cryst. 1997, 30, 565





_1097643391.unknown

