Crystal Structure Report for J Kovacs
Submitted by R Swartz 

Sample ID – CoIIITrenSOH
by W Kaminsky & R Swartz 
X-ray Crystallography Laboratory

University of Washington

01. November 2006
Data backup accessibly through http:

URL: 
http://cad4.cpac.washington.edu/structures
Username: 
xray-user

Password: 
hkl-data

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210 

Email: kaminsky@wintensor.com
Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures. Even I  have to pay for my own structures for my research.

A brown prism, size 0.15 x 0.12 x 0.07 mm was mounted on a glass capillary with oil.  Data was collected at -143oC with two sets of exposure as follows:

Scan 

Type
Scanlength (deg.)  start (deg.)
(     
(
(     
( 

1
      
(        
118.6




3.70
89.7
160  
 0 

2
      
(        
19.9




3.70
25.9
-175.0
 -74.1           

Crystal-to-detector distance was 30 mm and exposure time was 120 seconds per degree for all sets.  The scan width was 3o.   Data collection was 98.6% complete to 25.70o and 98.8% complete to 25o  in (.  A total of  15515 partial and complete reflections were collected covering the indices, h = -9 to 9, k = -17 to 17,  l = -22 to 22.  3656 reflections were symmetry independent and the Rint = 0.1611 indicated that the data was of less than average quality (0.07). 

Indexing and unit cell refinement indicated an orthorhombic P lattice.  The space group was found to be P 21 21 21 (No.19). 

The data was integrated and scaled using hkl-SCALEPACK. This program applies a multiplicative correction factor (S) to the observed intensities (I) and has the following form:


[image: image1.wmf]22

2(sin)/

S = ()/scale

B

e

ql

-


S is calculated from the scale and the B factor determined for each frame and is then applied to I to give the corrected intensity (Icorr).

Solution by direct methods (SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. 

All hydrogen atoms were located using a riding model. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares. 

Assignment of N5 and O1 was confirmed with a larger bond length between N5 and Co1 (1.939(9) Å) than previously reported for Co-O (1.899(2) Å; DSCoIIItrenTK). Further, by placing an oxygen instead of nitrogen for N5, the thermal parmeters increased significantly to be larger than those of Co1 and C12 which is physically unreasenable. In addition, O1 makes two hydrogen bonds, one is to N4, another to nitrogen of a symmetry related molecule, and no electron density was found around O1. The rest electron density was found to be smaller than a hydrogen would require.



_1097643391.unknown

