Crystal Structure Report for J Kovacs

Submitted by Dirk

Sample ID - DSCoIIItrenTK

by Kacey Claborn and Werner Kaminsky

X-ray Crystallography Laboratory

University of Washington

updated

06. March 2019
A black crystal block cut down to 0.19 x 0.17 x 0.14 mm was mounted on a glass capillary with oil.  Data was collected at -143oC with two sets of exposures as follows:

Scan 

Type
Scanlength (deg.)  start (deg.)
(     
(
(     
( 

1
      
(        
183.0




3.70
-1.5
160  
 0 

2                     (         104.9                                                2.06     48.97  105.07  -77.13

Crystal-to-detector distance was 30 mm and exposure time was 15 seconds per degree for all sets.  The scan width was 2o.   Data collection was 94.5% complete to 26.36o in (.  A total of  18295 partial and complete reflections were collected covering the indices, h = -9 to 8, k = -13 to 14, l = -15 to 14.  6556 reflections were symmetry independent and the Rint = 0.0408 indicated that the data was of better than average quality (0.07). 

Indexing and unit cell refinement indicated a triclinic P lattice.  The space group was found to be P-1 (No.2). 

The data was integrated and scaled using hkl-SCALEPACK. This program applies a multiplicative correction factor (S) to the observed intensities (I) and has the following form:

S = exp(2B(sinq/()2)/ scale

S is calculated from the scale and the B factor is determined for each frame and is then applied to I to give the corrected intensity (Icorr).

Solution by direct methods (SIR92) produced a complete heavy atom phasing model consistent with the proposed structure. 

All hydrogen atoms were located using a riding model. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares. 

[image: image1.wmf]O1

N2

N4

N3

S1

N1

Co1


� EMBED Word.Picture.8  ���








_1049174834.doc


O1







N2







N4







N3







S1







N1







Co1












