Crystal Structure Report for J Kovacs
by Maike Blakely & Werner Kaminsky

Sample Submitted by Erin Hanada 

ID – EH_01_4B_1
X-ray Crystallography Laboratory

University of Washington

04. April 2016
Data Collection  started: 3/28/2016

Documentation finished: 4/4/2016

Data backup accessibly through http:

URL: http://cad4.cpac.washington.edu/structures
W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210 

Email: kaminsky@chem.washington.edu
Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures. 

An orange prism, measuring 0.4 0.4 0.1 mm3 was mounted on a glass capillary with oil.  Data was collected at -173oC on a Bruker APEX II single crystal X-ray diffractometer, Mo-radiation.
Crystal-to-detector distance was 40 mm and exposure time was 30 seconds per degree for all sets.  The scan width was 0.5o.   Data collection was 100% complete to 25o  in (.  A total of  166395 (merged) reflections were collected covering the indices, -46<=h<=46, -12<=k<=12, -29<=l<=29.  12420 reflections were symmetry independent and the Rint = 0.0422 indicated that the data was brilliant.  Indexing and unit cell refinement indicated a primitive orthorhombic lattice.  The space group was found to be P b c n  (No. 60). 

The data was integrated and scaled using SAINT, SADABS within the APEX2 software package by Bruker.
 

Solution by direct methods (SHELXS, SIR97
) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL97.
,
 Scattering factors are from Waasmair and Kirfel
. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C---H distances in the range 0.95-1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares.
Nitrogen N2 is protonated to balance charge of the ligand and was positionally refined with riding displacement parameter.
The structure is of high quality and ready for publication. Table 1 summarizes the data collection details. Figure 1 shows an ORTEP
 of the asymmetric unit.
[image: image1.jpg]



Figure 1. ORTEP of the structure with thermal ellipsoids at the 50% probability level. 
Table 1: Crystallographic data for the structures provided.

Empirical formula 
C38 H61 N2 Na O3

Formula weight 
616.88

Temperature 
100(2) K

Wavelength 
0.71073 Å

Crystal system 
Orthorhombic

Space group 
P b c n

Unit cell dimensions
a = 34.9139(9) Å
= 90°.


b = 9.5442(3) Å
= 90°.


c = 22.1118(6) Å
 = 90°.

Volume
7368.2(4) Å3
Z
8

Density (calculated)
1.112 Mg/m3
Absorption coefficient
0.079 mm-1
F(000)
2704

Crystal size
0.40 x 0.40 x 0.10 mm3
Theta range for data collection
1.84 to 28.33°.

Index ranges
-46<=h<=46, -12<=k<=12, -29<=l<=29

Reflections collected
166394

Independent reflections
9173 [R(int) = 0.0422]

Completeness to theta = 25.00°
100.0 % 

Max. and min. transmission
0.9921 and 0.9691

Refinement method
Full-matrix least-squares on F2
Data / restraints / parameters
9173 / 1 / 400

Goodness-of-fit on F2
1.019

Final R indices [I>2sigma(I)]
R1 = 0.0423, wR2 = 0.1034

R indices (all data)
R1 = 0.0575, wR2 = 0.1124

Largest diff. peak and hole
0.349 and -0.249 e.Å-3



� Bruker (2007) APEX2 (Version 2.1-4), SAINT (version 7.34A), SADABS


(version 2007/4), BrukerAXS Inc, Madison, Wisconsin, USA.


� (a) Altomare, A.; Burla, C.; Camalli M.; Cascarano L.; Giacovazzo C.; Guagliardi A.;   Moliterni A.G.G.; Polidori G.; Spagna R. J. Appl. Cryst. 1999, 32, 115-119; (b) Altomare, A., Cascarano, G., Giacovazzo, C., Guagliardi, A., J. Appl. Cryst. 1993, 26, 343.


� Sheldrick, G. M. SHELXL-97: Program for the Refinement of Crystal Structures 1997 University of Gottingen, Germany.


� Mackay, S.; Edwards, C.; Henderson, A.; Gilmore, C.; Stewart, N.; Shankland, K.; Donald, A.; MaXus: a computer program for the solution and refinement of crystal structures from diffraction data. University of Glasgow, Scotland, 1997.


� Waasmaier, D.; Kirfel, A. Acta Crystallogr. A. 1995, 51, 416.


� Farrugia, L. J. Appl. Cryst. 1997, 30, 565





