Crystal Structure Report for K Goldberg

by Werner Kaminsky

Sample Submitted by Eirin Langseth 

ID – ELMe
X-ray Crystallography Laboratory

University of Washington

13. September 2012
Data backup accessibly through http:

URL: 
http://cad4.cpac.washington.edu/structures
Username: 
xray-user

Password: 
hkl-data

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210 

Email: kaminsky@chem.washington.edu
Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures. Even I  have to pay for my own structures for my research.

A clear needle, measuring 0.2 x 0.05 x 0.01 mm3 which was mounted on a loop with oil.  Data was collected at -173oC on a Bruker APEX II single crystal X-ray diffractometer, Mo-radiation. Crystal-to-detector distance was 40 mm and exposure time was 10 seconds per degree for all sets.  The scan width was 0.5o.   Data collection was 100% complete to 25o  in (.  The sample (Figure 1) showed signs of twinning. Additionally, twinning was indicated by the heterogeneity of birefringence and optical eigenray directions across the sample. 

[image: image1.png]


[image: image2.png]


[image: image3.png]



Figure 1. Crystal with signs of twinning, seen in (from left to right) transmission, birefringence and extinction
.

The raw data appeared indeed twinned. With CELL_NOW
 a 180o twin operation about  the reciprocal a-axis was found which, if unresolved, would cause considerable overlap of diffraction peak intensities from different domains of the sample. Multi-domain integration with SAINT within the APEX2 software package by Bruker
 and absorption correction with twinabs
 removed the overlap. A total of 13561 (merged) reflections were collected with 3503 symmetry independent reflections covering the indices, h = -13 to 13, k = -26 to 26,  l = -10 to 10 with Rint = 0.0690 indicated that the twin-refined data was good (average quality 0.07). Indexing and unit cell refinement indicated then a primitive monoclinic lattice.  The space group was found to be P 21/c  (No.14). 
Solution by direct methods (SHELXS, SIR97
) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL97.
,
 Scattering factors are from Waasmair and Kirfel
. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C(H distances in the range 0.95(1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares
Some residual electron density was observed close to the metal, which is a consequence of twinning.

The structure is of high quality and ready for publication. Table 1 summarizes the data collection details.. 
Figure 2 shows an ORTEP
 of the asymmetric unit with thermal ellipsoids at the 50% probability 
[image: image4.png]e
Lewo

u/‘ Y p>
s





Table 1: Crystallographic data for the structures provided.

Empirical formula 
C13 H13 Au Br N

Formula weight 
460.12

Temperature 
100(2) K

Wavelength 
0.71073 Å

Crystal system 
Monoclinic

Space group 
P 21/c

Unit cell dimensions
a = 9.3800(8) Å
= 90°.


b = 19.1064(16) Å
= 109.219(4)°.


c = 7.1404(6) Å
 = 90°.

Volume
1208.37(18) Å3
Z
4

Density (calculated)
2.529 Mg/m3
Absorption coefficient
15.451 mm-1
F(000)
848

Crystal size
0.20 x 0.03 x 0.01 mm3
Theta range for data collection
2.13 to 30.02°.

Index ranges
-13<=h<=13, -26<=k<=26, -10<=l<=10

Reflections collected
13561

Independent reflections
3503 [R(int) = 0.0690]

Completeness to theta = 25.00°
100.0 % 

Max. and min. transmission
0.8608 and 0.1481

Refinement method
Full-matrix least-squares on F2
Data / restraints / parameters
3503 / 0 / 148

Goodness-of-fit on F2
1.071

Final R indices [I>2sigma(I)]
R1 = 0.0427, wR2 = 0.0671

R indices (all data)
R1 = 0.0581, wR2 = 0.0712

Extinction coefficient
0.00016(6)

Largest diff. peak and hole
2.438 and -2.475 e.Å-3
� W. Kaminsky, E. Gunn, R. Sours, B. Kahr: Simultaneous false-color imaging of birefringence, extinction, and transmittance at camera speed. J Microscopy. 228 (2008) 153-164. 


   W. Kaminsky: Real-time linear-birefringence-detecting polarization microscope. April 21st 2009, US Patent 7522278.


� Sheldrick, G. M. (2005). CELL_NOW. University of Goettingen, Germany.


� Bruker (2007) APEX2 (Version 2.1-4), SAINT (version 7.34A), SADABS


(version 2007/4), BrukerAXS Inc, Madison, Wisconsin, USA.


� Sheldrick, G. M. (2007). TWINABS. University of Goettingen, Germany.


� (a) Altomare, A.; Burla, C.; Camalli M.; Cascarano L.; Giacovazzo C.; Guagliardi A.;   Moliterni A.G.G.; Polidori G.; Spagna R. J. Appl. Cryst. 1999, 32, 115-119; (b) Altomare, A., Cascarano, G., Giacovazzo, C., Guagliardi, A., J. Appl. Cryst. 1993, 26, 343.


� Sheldrick, G. M. SHELXL-97: Program for the Refinement of Crystal Structures 1997 University of Gottingen, Germany.


� Mackay, S.; Edwards, C.; Henderson, A.; Gilmore, C.; Stewart, N.; Shankland, K.; Donald, A.; MaXus: a computer program for the solution and refinement of crystal structures from diffraction data. University of Glasgow, Scotland, 1997.


� Waasmaier, D.; Kirfel, A. Acta Crystallogr. A. 1995, 51, 416.


� Farrugia, L. J. Appl. Cryst. 1997, 30, 565





