Crystal Structure Report for K Goldberg

Submitted by Greg Fulmer 

Sample ID – GRF001

by Rodney Swartz & W.K

X-ray Crystallography Laboratory

University of Washington

07. July 2008
Data backup accessibly through http:

URL: 
http://cad4.cpac.washington.edu/structures
Username: 
xray-user

Password: 
hkl-data

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210 

Email: kaminsky@wintensor.com
Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures. Even I  have to pay for my own structures for my research.

A red prism of size 0.43 x 0.29 x 0.22 was mounted on a glass capillary with oil.  Data was collected at -143oC with six sets of exposure as follows:

Scan 

Type
Scanlength (deg.)  start (deg.)
(     
(
(     
( 

1
      
(        
183.6




3.70
9.70
160  
 0 

2
      
(        
9.9




3.70
25.9
-159.9 
 -74.1           

Crystal-to-detector distance was 30 mm and exposure time was 60 seconds per degree for all sets.  The scan width was 1o.   Data collection was 97.2% complete to 28.28o in ( and 99.7% complete to 25o.  A total of 35,579 partial and complete reflections were collected covering the indices, h = -12 to 12, k = -19 to 19,  l = -23 to 23.  3,721 reflections were symmetry independent and the Rint = 0.0 indicated that the data was above average quality (0.07). 

Indexing and unit cell refinement indicated a triclinic lattice.  The space group was found to be P 21 21 21 (No. 19). 

The data was integrated and scaled using hkl-SCALEPACK. This program applies a multiplicative correction factor (S) to the observed intensities (I) and has the following form:


[image: image1.wmf]22

2(sin)/

S = ()/scale

B

e

ql

-


S is calculated from the scale and the B factor determined for each frame and is then applied to I to give the corrected intensity (Icorr).

Solution by direct methods (SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. 

All hydrogen atoms were located using a riding model. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares. 




_1097643391.unknown

