Crystal Structure Report for K Goldberg
Submitted by Greg Fulmer 

Sample ID – GRF005
by Werner Kaminsky

X-ray Crystallography Laboratory

University of Washington

15. September 2009
Data backup accessibly through http:

URL: 
http://cad4.cpac.washington.edu/structures
Username: 
xray-user

Password: 
hkl-data

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210 

Email: kaminsky@chem.washington.edu
Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures. Even I  have to pay for my own structures for my research.

A colorless prism, 0.36 x 0.24 x 0.12 mm of size with signs of inseparable twinning was mounted on a glass capillary with oil.  Data was collected at -143oC.
Crystal-to-detector distance was 35 mm and exposure time was 50 seconds per degree for all sets.  The scan width was 1o.   Data collection was 94.3% complete to 25o  in (.  A total of  50131 partial and complete reflections were collected covering the indices, h = -30 to 30, k = -18 to 19,  l = -14 to 14.  4355 reflections were symmetry independent and the Rint = 0.1696 indicated a slight impact of twinning (average quality 0.07). 

Indexing and unit cell refinement indicated a monoclinic C lattice.  The space group was found to be C 2/c (No.15). 

The data was integrated and scaled using hkl-SCALEPACK. This program applies a multiplicative correction factor (S) to the observed intensities (I) and has the following form:


[image: image1.wmf]22

2(sin)/

S = ()/scale

B

e

ql

-


S is calculated from the scale and the B factor determined for each frame and is then applied to I to give the corrected intensity (Icorr).

Solution by direct methods (SIR97) produced a complete heavy atom phasing model with motives of the proposed structure.
All hydrogen atoms were located using a riding model. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares. 

The structure is publishable with most of the twinning problems removed. Thermal parameters of some carbon atoms had to be restraint for that reason.
The dimmer exhibits a twofold rotation with one half created through this symmetry out of the other.




_1097643391.unknown

