Crystal Structure Report for Jenekhe

Submitted by Yan 

Sample ID – HPQ
by Werner Kaminsky

X-ray Crystallography Laboratory

University of Washington

29. September 2006
Data backup accessibly through ftp:

computer: 

chmraypc.cpac.washington.edu

login: 

anonymous

password:

(your name or email address)

location: 
c:\structures\jenekhe\PeiTzuWu\HPQ\HPQ.htm
Data backup accessibly through http:

URL: 
http://cad4.cpac.washington.edu/structures/jenekhe/PeiTzuWu/HPQ/HPQ.htm
Username: 
xray-user

Password: 
hkl-data

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210 

Email: kaminsky@wintensor.com
Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures. Even I  have to pay for my own structures for my research.

A yellow crystal plate size 0.50 x 0.34 x 0.24 mm was mounted on a glass capillary with oil.  Data was collected at -143oC with four sets of exposure as follows:

Scan 

Type
Scanlength (deg.)  start (deg.)
(     
(
(     
( 

1
      
(        
183.0




3.7
-1.5
160  
 0 

2
      
(        
106.5




3.7
-145.9
-200.1
 74.1           

2
      
(        
76.5




3.7
-25.9
-200.1
 74.1           

2
      
(        
46.5




3.7
94.1
-180.1
 74.1           

Crystal-to-detector distance was 30 mm and exposure time was 7 seconds per degree for all sets.  The scan width was 2o.   Data collection was 99.5% complete to 25o  in (.  A total of  17763 partial and complete reflections were collected covering the indices, h = -6 to 7, k = -13 to 13,  l = -14 to 14. 2781 reflections were symmetry independent and the Rint = 0.0680 indicated that the data was of average quality (0.07). 

Indexing and unit cell refinement indicated a triclinic lattice.  The space group was found to be P(1 (No.2). 

The data was integrated and scaled using hkl-SCALEPACK. This program applies a multiplicative correction factor (S) to the observed intensities (I) and has the following form:

S = exp(2B(sinq/()2)/ scale

S is calculated from the scale and the B factor is determined for each frame and is then applied to I to give the corrected intensity (Icorr).

Solution by direct methods (SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. 

All hydrogen atoms with the exception of the hydroxy-hydrogen H1 were located using a riding model. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares. 

The hydrogen bond between O1 and N1 is characterized by

 D-H...A                      d(D-H)      d(H...A)    d(D...A)    <(DHA)

 O(1)-H(1)...N(1)             0.939(19)   1.62(2)     2.5280(18)  160.2(17)

 ____________________________________________________________________________

the structure was checked with checkcif (http://journals.iucr.org/services/cif/checking/checkform.html) and produced no warnings.



