Crystal Structure Report for  Sigurdson

Submitted by Mebbie

Sample ID – I104B-lowT

by Kacey Claborn and Werner Kaminsky

X-ray Crystallography Laboratory

University of Washington

01. June 2001
Data backup accessibly through ftp:

computer: 

chmraypc.cpac.washington.edu

login: 

anonymous

password:

(your name or email address)

location: 
c:\structures\ sigurdson\mebbie\I104Bdata3

A clear crystal prism, size  0.22 x 0.05 x 0.05 mm was mounted on a glass capillary with epoxy.  

The crystal was indexed by x-rays, giving the following graph:

[image: image1.wmf]C4

C3

C2

C5

C6

C1

N1

O1

C7

C10

C8

N2

C9

O2

N3

C11

C12

O3

C13

C14

O4

C15

O5

C18

C19

C20

C21

C17

C16

N4

C23

N5

C24

O7

N6

C25

C22

O6

C26

O8

C27

C29

C28

O10

C30

O9


The twofold b-axis is parallel to the long-axis of the crystal. The b-axis is also the shortest of the three (a=11.897Ă, b=6.248 Ă, c=19.274 Ă) and growth was expected to be fastest along b, which is also a screw-axis.

Data was collected at 130K with one set of exposure as follows:

Scan 

Type
Scanlength (deg.)  start (deg.)
(     
(
(     
( 

1
      
(        
182.0




3.70
-40.5
160  
 0      

Crystal-to-detector distance was 30 mm and exposure time was 120 seconds per degree for all sets.  The scan width was 1.3o.   Data collection was 70.6% complete to 26.09o in (.  A total of   17929 partial and complete reflections were collected covering the indices, h = -14 to 14, k = -6 to 7, l = -23 to 22.  3031 reflections were symmetry independent and the Rint = 0.0680 indicated that the data was about average quality (0.07). 

Indexing and unit cell refinement indicated a monoclinic P lattice.  The space group was found to be P21. 

The data was integrated and scaled using hkl-SCALEPACK. This program applies a multiplicative correction factor (S) to the observed intensities (I) and has the following form:

S = exp(2B(sinq/()2)/ scale

S is calculated from the scale and the B factor is determined for each frame and is then applied to I to give the corrected intensity (Icorr).

Solution by direct methods (SHELXS97) produced an almost complete heavy atom phasing model consistent with the proposed structure. 

All hydrogen atoms were located using a riding model. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares. 

The structure at 130K

[image: image2.emf]
Data was also collected at room temperature. The structure showed some degree of disorder represented in C13a-C13b, and O4a-O4b.

[image: image3.wmf]O5

C15

C13b

C13a

C12

C11

C14

O3

O4a

O4b

N3

O2

C9

C10

C7

O1

C6

C1

N1

C8

N2

C5

C4

C3

C2

O7

C24

N5

C23

N4

C16

C17

C18

C19

C20

C21

O6

C22

C25

N6

C26

C27

O8

O10

C28

C29

O9

C30


�





�





(100)





(001)





(111)





�








