Crystal Structure Report for K Goldberg

by Maike Blakely & Werner Kaminsky

Sample Submitted by A. Phearman 

ID – IRM_I_92

X-ray Crystallography Laboratory

University of Washington

08. August 2017
Data Collection  started: 7/24/2017
Documentation finished: 8/8/2017
Data backup accessibly through http:

URL: http://cad4.cpac.washington.edu/structures
W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210 

Email: kaminsky@chem.washington.edu
Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures. 

A dark red prism, measuring 0.03 x 0.03 x 0.03 mm3 was mounted on a loop with oil.  Data was collected at -173oC on a Bruker APEX II single crystal X-ray diffractometer, Mo-radiation.
Crystal-to-detector distance was 40 mm and exposure time was 240 seconds per frame for all sets.  The scan width was 1o.   Data collection was 99.4% complete to 25o  in (.  A total of  18024 reflections were collected covering the indices, -17<=h<=17, -29<=k<=29, -19<=l<=19.  9129 reflections were symmetry independent and the elevated Rint = 0.1586 reflects an extremely small sample size.  Indexing and unit cell refinement indicated a primitive monoclinic lattice.  The space group was found to be P 21/c  (No. 14). 

The data was integrated and scaled using SAINT, SADABS within the APEX2 software package by Bruker.
 

Solution by direct methods (SHELXS, SIR97
) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL97.
,
 Scattering factors are from Waasmair and Kirfel
. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C---H distances in the range 0.95-1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares.
The structure contains one toluene solvent molecule which appears not to be disordered. However, except for the two Pd atoms, all other structural features are disordered into two overlapping representations of the molecule. A similar structure was determined just recently,
 however, the solvent there was benzene. 
The structure is of high quality and ready for publication. Table 1 summarizes the data collection details. Figure 1 shows an ORTEP
 of the asymmetric unit.
[image: image1.jpg]o/%\ K /M“/

475 15





Figure 1. ORTEP of the structure with thermal ellipsoids at the 50% probability level. Disorder omitted for clarity.

Table 1: Crystallographic data for the structures provided.

Empirical formula 
C58 H50 O3 Pd2

Formula weight 
1007.78

Temperature 
100(2) K

Wavelength 
0.71073 Å

Crystal system 
Monoclinic

Space group 
P 21/c

Unit cell dimensions
a = 13.6772(12) Å
= 90°.


b = 23.483(2) Å
= 113.687(6)°.


c = 15.2881(16) Å
 = 90°.

Volume
4496.6(7) Å3
Z
4

Density (calculated)
1.489 Mg/m3
Absorption coefficient
0.846 mm-1
F(000)
2056

Crystal size
0.03 x 0.03 x 0.03 mm3
Theta range for data collection
1.69 to 26.37°.

Index ranges
-17<=h<=17, -29<=k<=29, -19<=l<=19

Reflections collected
18024

Independent reflections
9129 [R(int) = 0.1586]

Completeness to theta = 25.00°
99.4 % 

Max. and min. transmission
0.9751 and 0.9751

Refinement method
Full-matrix least-squares on F2
Data / restraints / parameters
9129 / 791 / 686

Goodness-of-fit on F2
0.942

Final R indices [I>2sigma(I)]
R1 = 0.0663, wR2 = 0.1230

R indices (all data)
R1 = 0.1861, wR2 = 0.1606

Largest diff. peak and hole
0.686 and -1.242 e.Å-3
� Bruker (2007) APEX2 (Version 2.1-4), SAINT (version 7.34A), SADABS (version 2007/4), BrukerAXS Inc, Madison, Wisconsin, USA.


� (a) Altomare A, Burla C, Camalli M, Cascarano G L, Giacovazzo C, Guagliardi A,   Moliterni AGG, Polidori G, Spagna R. (1999) SIR97: a new tool for crystal structure determination and refinement Journal of Applied Crystallography, 32, 115-119. 


   (b) Altomare A, Cascarano G L, Giacovazzo C, Guagliardi A. (1993) Completion and refinement of crystal structures with SIR 92. Journal of Applied Crystallography, 26, 343-350.


� (a) Sheldrick GM. (1997) SHELXL-97, Program for the Refinement of Crystal Structures. University of Göttingen, Germany.


   (b) Sheldrick GM. (2013) Crystal structure refinement with SHELXL. Acta Cryst. (2015). C71, 3-8.


� Mackay, S.; Edwards, C.; Henderson, A.; Gilmore, C.; Stewart, N.; Shankland, K.; Donald, A. (1997) MaXus: a computer program for the solution and refinement of crystal structures from diffraction data. University of Glasgow, Scotland,.


� Waasmaier, D.; Kirfel, A. (1995) New Analytical Scattering Factor Functions for Free Atoms and Ions. Acta Crystallographica A., 51, 416-430.


� A.R.Kapdi, A.C.Whitwood, D.C.Williamson, J.M.Lynam, M.J.Burns, T.J.Williams, A.J.Reay, J.Holmes, I.J.S.Fairlamb; J.Am.Chem.Soc. (2013), 135, 8388, doi:10.1021/ja403259c


� Farrugia LJ. (1997) Ortep-3 for Windows. Journal of Applied Crystallography, 30, 565





