Crystal Structure Report for K. Goldberg

by Tom Porter & Werner Kaminsky

Sample Submitted by Kate Allen 

ID – KEA030
X-ray Crystallography Laboratory

University of Washington

02. July 2013
Data backup accessibly through http:

URL: 
http://cad4.cpac.washington.edu/structures
Username: 
xray-user

Password: 
hkl-data

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210 

Email: kaminsky@chem.washington.edu
Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures. Even I  have to pay for my own structures for my research.

From a batch of small orange conglomerates was taken an inseparably twinned sample, measuring 0.14 x 0.12 x 0.05 mm3 which was mounted on a loop with oil.  Data was collected at -173oC on a Bruker APEX II single crystal X-ray diffractometer, Mo-radiation. Crystal-to-detector distance was 40 mm and exposure time was 30 seconds per degree for all sets.  The scan width was 0.5o.   Data collection was 99.8% complete to 25o  in (.  
With CELL_NOW
 two datasets associated to the two individuals of the conglomerate were found which, if unresolved, would cause considerable overlap of diffraction peak intensities. Multi-domain integration with SAINT within the APEX2 software package by Bruker
 and absorption correction with twinabs
 removed the overlap. A total of 8297 symmetry independent reflections were collected covering the indices, h = -11 to 12, k = -15 to 16,  l = 0 to 20. The Rint = 0.0847 showed that the twin-refined data was acceptable (average quality 0.07). Indexing and unit cell refinement indicated then a triclinic P lattice.  The space group was found to be P(1  (No.2). 

Solution by direct methods (SHELXS, SIR97
) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL97.
,
 Scattering factors are from Waasmair and Kirfel
. 
Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C(H distances in the range 0.95(1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares
The structure consists of two molecules in the asymmetric unit, which are approximately related by inversion symmetry in addition to the inversion operation of the triclinic space group. Twinning in two carboxylic ligands was resolved explicitly, but the impact from that disorder on the hydrogen-bonded water was only visible in slightly elongated displacement parameters of the water oxygen and not further dissected.
The structure is of high quality and ready for publication. Table 1 summarizes the data collection details. 
[image: image1.png]


 
Figure 1: ORTEP
 of the asymmetric unit with thermal ellipsoids at the 50% probability (disorder omitted for clarity). 
Table 1: Crystallographic data for the structures provided.

Identification code 
twin4_2

Empirical formula 
C36 H56 O5.16 P2 Pd

Formula weight 
739.71

Temperature 
100(2) K

Wavelength 
0.71073 Å

Crystal system 
Triclinic

Space group 
P -1

Unit cell dimensions
a = 8.4191(4) Å
= 71.585(2)°.


b = 9.7162(4) Å
= 70.990(3)°.


c = 11.8675(5) Å
 = 73.491(2)°.

Volume
852.87(6) Å3
Z
1

Density (calculated)
1.440 Mg/m3
Absorption coefficient
0.680 mm-1
F(000)
389.6

Crystal size
0.15 x 0.07 x 0.04 mm3
Theta range for data collection
2.26 to 25.35°.

Index ranges
-10<=h<=10, -11<=k<=11, -14<=l<=14

Reflections collected
5771

Independent reflections
2947 [R(int) = 0.0424]

Completeness to theta = 25.00°
94.2 % 

Max. and min. transmission
0.9733 and 0.9049

Refinement method
Full-matrix least-squares on F2
Data / restraints / parameters
2947 / 96 / 273

Goodness-of-fit on F2
1.146

Final R indices [I>2sigma(I)]
R1 = 0.0528, wR2 = 0.1043

R indices (all data)
R1 = 0.0726, wR2 = 0.1095

Largest diff. peak and hole
0.722 and -0.723 e.Å-3
� Sheldrick, G. M. (2005). CELL_NOW. University of Goettingen, Germany.


� Bruker (2007) APEX2 (Version 2.1-4), SAINT (version 7.34A), SADABS


(version 2007/4), BrukerAXS Inc, Madison, Wisconsin, USA.


� Sheldrick, G. M. (2007). TWINABS. University of Goettingen, Germany.


� (a) Altomare, A.; Burla, C.; Camalli M.; Cascarano L.; Giacovazzo C.; Guagliardi A.;   Moliterni A.G.G.; Polidori G.; Spagna R. J. Appl. Cryst. 1999, 32, 115-119; (b) Altomare, A., Cascarano, G., Giacovazzo, C., Guagliardi, A., J. Appl. Cryst. 1993, 26, 343.


� Sheldrick, G. M. SHELXL-97: Program for the Refinement of Crystal Structures 1997 University of Gottingen, Germany.


� Mackay, S.; Edwards, C.; Henderson, A.; Gilmore, C.; Stewart, N.; Shankland, K.; Donald, A.; MaXus: a computer program for the solution and refinement of crystal structures from diffraction data. University of Glasgow, Scotland, 1997.


� Waasmaier, D.; Kirfel, A. Acta Crystallogr. A. 1995, 51, 416.


� Farrugia, L. J. Appl. Cryst. 1997, 30, 565





