Crystal Structure Report for B. Cossairt
by Dylan Rogers & Werner Kaminsky

Sample Submitted by Cecilia Johnson 

ID – MCJ_1Z_3a_4
X-ray Crystallography Laboratory

University of Washington

03. May 2019
Data Collection  started: 05/01/19
Documentation finished: 05/03/19
Data backup accessibly through http:

URL: http://cad4.cpac.washington.edu/structures
W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210 

Email: kaminsky@chem.washington.edu
Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures. 

A clear needle, measuring 0.26 x 0.05 x 0.03 mm3 was mounted on a loop with oil.  Data was collected at -173oC on a Bruker APEX II single crystal X-ray diffractometer, Mo-radiation.
Crystal-to-detector distance was 40 mm and exposure time was 60 seconds per frame for all sets.  The scan width was 1.0o.   Data collection was 100% complete to 25o  in (.  A total of 23933 reflections were collected covering the indices, -18<=h<=18, -25<=k<=25, 0<=l<=24.  12142 reflections were symmetry independent and the Rint = 0.2302 indicated that the data was of worse than average quality (0.07).  Indexing and unit cell refinement indicated a primitive monoclinic lattice.  The space group was found to be P 21/n  (No.14). 

The data was integrated and scaled using SAINT, SADABS within the APEX2 software package by Bruker.
 

Solution by direct methods (SHELXT
 or SIR97
) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL.
,
 Scattering factors are from Waasmair and Kirfel
. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C---H distances in the range 0.95-1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares.
The ruthenium complex is accompanied by two hexafluorophosphate anions and one dichlormethane solvent molecule.
The structure is of high quality and ready for publication. Table 1 summarizes the data collection details. Figure 1 shows an ORTEP
 of the asymmetric unit.
[image: image1.jpg]



Figure 1. ORTEP of the structure with thermal ellipsoids at the 50% probability level. 

Table 1: Crystallographic data for the structures provided.

Empirical formula 
C57 H60 Cl2 F12 N5 P5 Ru

Formula weight 
1369.92

Temperature 
100(2) K

Wavelength 
0.71073 Å

Crystal system 
Monoclinic

Space group 
P 21/n

Unit cell dimensions
a = 14.873(6) Å
= 90°.


b = 20.764(7) Å
= 91.306(15)°.


c = 19.236(7) Å
 = 90°.

Volume
5939(4) Å3
Z
4

Density (calculated)
1.532 Mg/m3
Absorption coefficient
0.569 mm-1
F(000)
2792

Crystal size
0.260 x 0.050 x 0.030 mm3
Theta range for data collection
1.443 to 26.370°.

Index ranges
-18<=h<=18, -25<=k<=25, 0<=l<=24

Reflections collected
23933

Independent reflections
12142 [R(int) = 0.2302]

Completeness to theta = 25.000°
100.0 % 

Refinement method
Full-matrix least-squares on F2
Data / restraints / parameters
12142 / 57 / 766

Goodness-of-fit on F2
0.710

Final R indices [I>2sigma(I)]
R1 = 0.0668, wR2 = 0.1205

R indices (all data)
R1 = 0.2301, wR2 = 0.1740

Largest diff. peak and hole
1.196 and -1.081 e.Å-3
� Bruker (2007) APEX2 (Version 2.1-4), SAINT (version 7.34A), SADABS (version 2007/4), BrukerAXS Inc, Madison, Wisconsin, USA.


� Sheldrick GM. (2015) SHELXT - Integrated space-group and crystal-structure determination. Acta Cryst. A71, 3-8.


� (a) Altomare A, Burla C, Camalli M, Cascarano G L, Giacovazzo C, Guagliardi A,   Moliterni AGG, Polidori G, Spagna R. (1999) SIR97: a new tool for crystal structure determination and refinement Journal of Applied Crystallography, 32, 115-119. 


   (b) Altomare A, Cascarano G L, Giacovazzo C, Guagliardi A. (1993) Completion and refinement of crystal structures with SIR 92. Journal of Applied Crystallography, 26, 343-350.


� (a) Sheldrick GM. (1997) SHELXL-97, Program for the Refinement of Crystal Structures. University of Göttingen, Germany.


   (b) Sheldrick GM. (2015) Crystal structure refinement with SHELXL. Acta Cryst. (2015). C71, 3–8


� Mackay, S.; Edwards, C.; Henderson, A.; Gilmore, C.; Stewart, N.; Shankland, K.; Donald, A. (1997) MaXus: a computer program for the solution and refinement of crystal structures from diffraction data. University of Glasgow, Scotland,.


� Waasmaier, D.; Kirfel, A. (1995) New Analytical Scattering Factor Functions for Free Atoms and Ions. Acta Crystallographica A., 51, 416-430.


� Farrugia LJ. (1997) Ortep-3 for Windows. Journal of Applied Crystallography, 30, 565





