Crystal Structure Report for B Cossairt

by Dylan Rogers & Werner Kaminsky

Sample Submitted by Cecilia Johnson 

ID – MCJ_3b_66

X-ray Crystallography Laboratory

University of Washington

21. December 2020
Data Collection  started: 12/12/2020
Documentation finished: 12/21/2020
Data backup accessibly through http:

URL: http://cad4.cpac.washington.edu/structures
W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210 

Email: kaminsky@chem.washington.edu
Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures. 

A red piece , measuring 0.09 x 0.06 x 0.05 mm3 was mounted on a loop with oil.  Data was collected at -173oC on a Bruker APEX II single crystal X-ray diffractometer, Mo-radiation.
Crystal-to-detector distance was 40 mm and exposure time was 60 seconds per frame for all sets.  The scan width was 0.5o.   Data collection was 100% complete to 25o  in (.  A total of  31252 merged reflections were collected covering the indices, -15<=h<=15, -15<=k<=15, -33<=l<=33.  15635 reflections were symmetry independent and the Rint = 0.1327 indicated that the data was of appropriate.  Indexing and unit cell refinement indicated a triclinic lattice.  The space group was found to be P(1  (No. 2). 

Solution by direct methods (SHELXS, SIR97
) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL97.
,
 Scattering factors are from Waasmair and Kirfel
. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C---H distances in the range 0.95-1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares.
The hydrogen bridged ruthenium dimer is accompanied by 4 disordered THF molecules and one disordered PF6ˉ anion.

In addition, two disordered hydrogen bonds are observed between nitrogens.

Due to disorder, restraints were applied to stabilize the refinement.

The structure is of high quality and ready for publication. Table 1 summarizes the data collection details. Figure 1 shows an ORTEP
 of the asymmetric unit.
[image: image1.jpg]



Figure 1. ORTEP of the structure with thermal ellipsoids at the 50% probability level. Disorder and solvent omitted for clarity.

Table 1: Crystallographic data for the structures provided.

Empirical formula 
C92 H109 F6 N12 O4 P3 Ru2

Formula weight 
1855.96

Temperature 
100(2) K

Wavelength 
0.71073 Å

Crystal system 
Triclinic

Space group 
P -1

Unit cell dimensions
a = 12.9219(12) Å
a= 82.215(4)°.


b = 13.0307(11) Å
b= 83.087(4)°.


c = 27.997(2) Å
g = 66.365(4)°.

Volume
4267.6(6) Å3
Z
2

Density (calculated)
1.444 Mg/m3
Absorption coefficient
0.483 mm-1
F(000)
1928

Crystal size
0.090 x 0.060 x 0.050 mm3
Theta range for data collection
1.472 to 25.350°.

Index ranges
-15<=h<=15, -15<=k<=15, -33<=l<=33

Reflections collected
31252

Independent reflections
15635 [R(int) = 0.1327]

Completeness to theta = 25.000°
100.0 % 

Refinement method
Full-matrix least-squares on F2
Data / restraints / parameters
15635 / 905 / 1107

Goodness-of-fit on F2
0.948

Final R indices [I>2sigma(I)]
R1 = 0.0571, wR2 = 0.0926

R indices (all data)
R1 = 0.1504, wR2 = 0.1193

Largest diff. peak and hole
0.729 and -0.737 e.Å-3
� (a) Altomare A, Burla C, Camalli M, Cascarano G L, Giacovazzo C, Guagliardi A,   Moliterni AGG, Polidori G, Spagna R. (1999) SIR97: a new tool for crystal structure determination and refinement Journal of Applied Crystallography, 32, 115-119. 


   (b) Altomare A, Cascarano G L, Giacovazzo C, Guagliardi A. (1993) Completion and refinement of crystal structures with SIR 92. Journal of Applied Crystallography, 26, 343-350.


� (a) Sheldrick GM. (1997) SHELXL-97, Program for the Refinement of Crystal Structures. University of Göttingen, Germany.


   (b) Sheldrick GM. (2013) Crystal structure refinement with SHELXL. Acta Cryst. (2015). C71, 3-8.


� Mackay, S.; Edwards, C.; Henderson, A.; Gilmore, C.; Stewart, N.; Shankland, K.; Donald, A. (1997) MaXus: a computer program for the solution and refinement of crystal structures from diffraction data. University of Glasgow, Scotland,.


� Waasmaier, D.; Kirfel, A. (1995) New Analytical Scattering Factor Functions for Free Atoms and Ions. Acta Crystallographica A., 51, 416-430.


� Farrugia LJ. (1997) Ortep-3 for Windows. Journal of Applied Crystallography, 30, 565





