Crystal Structure Report for J. Kovacs
by Michael Coggins and Werner Kaminsky
Sample Submitted by Michael Coggins 

ID – michael023
X-ray Crystallography Laboratory

University of Washington

29. October 2010
Data backup accessibly through http:

URL: 
http://cad4.cpac.washington.edu/structures
Username: 
xray-user

Password: 
hkl-data

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210 

Email: kaminsky@chem.washington.edu
Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures. Even I  have to pay for my own structures for my research.

A red prism measuring 0.15 x 0.15 x 0.10 mm3 was mounted on a glass capillary with oil.  Data was collected at -173 oC on a Bruker APEX II single crystal X-ray diffractometer, Mo-radiation.
Crystal-to-detector distance was 40 mm and exposure time was 10 seconds per degree for all sets.  The scan width was 0.5o.   Data collection was 100 % complete to 25o  in (.  A total of 67168 (merged) reflections were collected covering the indices, h = -10 to 10, k = -16 to 16,  l = -23 to 23.  4653 reflections were symmetry independent and the Rint = 0.0523 indicated that the data was good (average quality 0.07).  Indexing and unit cell refinement indicated an orthorhombic P lattice.  The space group was found to be P 21 21 21. 

The data was integrated and scaled using SAINT, SADABS within the APEX2 software package by Bruker.
 

Solution by direct methods (SHELXS, SIR97
) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL97.
,
 Scattering factors are from Waasmair and Kirfel
. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C---H distances in the range 0.95-1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares.
The structure is of high quality and ready for publication. Table 1 summarizes the data collection details. Figure 1 shows an ORTEP
 of the asymmetric unit.
[image: image1.png]-35Y

(290610)

PLATON-Oct 5 22:51:43 2010

N

-97

NOMOVE FORCED

michael 023P 21 21 21

R =0.02

RES=

Prob = 50
Temp = 100
0 -109 X





Figure 1. ORTEP of the structure with thermal ellipsoids at the 50% probability level. 
Table 1: Crystallographic data for the structures provided.

Identification code 
michael023_0m

Empirical formula 
C11 H25 Co F6 N4 P S

Formula weight 
449.31

Temperature 
100(2) K

Wavelength 
0.71073 Å

Crystal system 
Orthorhombic

Space group 
P 21 21 21

Unit cell dimensions
a = 8.1657(3) Å
 = 90°.


b = 12.6922(4) Å
 = 90°.


c = 17.9418(6) Å
  = 90°.

Volume
1859.50(11) Å3

Z
4

Density (calculated)
1.605 Mg/m3

Absorption coefficient
1.179 mm-1

F(000)
924

Crystal size
0.15 x 0.15 x 0.10 mm3

Theta range for data collection
1.97 to 28.41°.

Index ranges
-10<=h<=10, -16<=k<=16, -23<=l<=23

Reflections collected
67168

Independent reflections
4653 [R(int) = 0.0523]

Completeness to theta = 25.00°
100.0 % 

Max. and min. transmission
0.8912 and 0.8430

Refinement method
Full-matrix least-squares on F2

Data / restraints / parameters
4653 / 0 / 220

Goodness-of-fit on F2
1.059

Final R indices [I>2sigma(I)]
R1 = 0.0237, wR2 = 0.0459

R indices (all data)
R1 = 0.0288, wR2 = 0.0475

Absolute structure parameter
0.005(9)

Largest diff. peak and hole
0.278 and -0.222 e.Å-3




� Bruker (2007) APEX2 (Version 2.1-4), SAINT (version 7.34A), SADABS


(version 2007/4), BrukerAXS Inc, Madison, Wisconsin, USA.


� (a) Altomare, A.; Burla, C.; Camalli M.; Cascarano L.; Giacovazzo C.; Guagliardi A.;   Moliterni A.G.G.; Polidori G.; Spagna R. J. Appl. Cryst. 1999, 32, 115-119; (b) Altomare, A., Cascarano, G., Giacovazzo, C., Guagliardi, A., J. Appl. Cryst. 1993, 26, 343.


� Sheldrick, G. M. SHELXL-97: Program for the Refinement of Crystal Structures 1997 University of Gottingen, Germany.


� Mackay, S.; Edwards, C.; Henderson, A.; Gilmore, C.; Stewart, N.; Shankland, K.; Donald, A.; MaXus: a computer program for the solution and refinement of crystal structures from diffraction data. University of Glasgow, Scotland, 1997.


� Waasmaier, D.; Kirfel, A. Acta Crystallogr. A. 1995, 51, 416.


� Farrugia, L. J. Appl. Cryst. 1997, 30, 565





