Crystal Structure Report for K. Goldberg

Submitted by Scott William

Sample ID - Pt4OMe

by Werner Kaminsky

X-ray Crystallography Laboratory

University of Washington

22. June 2004
A clear crystal prism 0.1 x 0.3 x 0.18 mm was mounted on a glass capillary with epoxy.  Data was collected at 20oC with two sets of exposures as follows:

Scan 

Type
Scanlength (deg.)  start (deg.)
(     
(       
(     
( 

1
      
(        
182                                              
2.21    
-1.5  
160     
0      

2
      
(        
29                                          
-1.5 
-49.3  
-164.5
-134.7 

Crystal-to-detector distance was 27 mm and exposure time was 20 seconds for all sets.  The scan width was 1.8o.   Data collection was 94% complete to 26.35o in (.  A total of  27377 partial and complete reflections were collected covering the indices, h = -25 to 24, k = -11 to 12, l = -22 to 23.  4456 reflections were symmetry independent and the Rint = 0.0659 indicated that the quality of data was good. 

Indexing and unit cell refinement indicated a monoclinic P lattice.  The space group was found to be P21/c.  Analysis of the normalized structure factors indicated a centric cell favoring above symmetry. 

The data was integrated and scaled using hkl-SCALEPACK.  Absorption correction was performed using SORTAV.

Solution by direct methods (SHELXS97) produced a complete heavy atom phasing model consistent with the proposed structure submitted. 

All hydrogen were located using a riding model. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares. 

A disordered toluene molecule was found at a site occupancy of 50%. 

