Crystal Structure Report for J Mayer

Submitted by Rebecca Hayoun 

Sample ID – rebecca01

by Rodney Swartz & Werner Kaminsky

X-ray Crystallography Laboratory

University of Washington

19. March 2009
Data backup accessibly through http:

URL: 
http://cad4.cpac.washington.edu/structures
Username: 
xray-user

Password: 
hkl-data

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210 

Email: kaminsky@wintensor.com
Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures. Even I  have to pay for my own structures for my research.

A red prism of size 0.15 x 0.20 x 0.50 was mounted on a glass capillary with oil.  Data was collected at 295K and 130K. We present here the low_T data.

Crystal-to-detector distance was 30 mm and exposure time was 30 seconds per degree for all sets.  The scan width was 1.0o.   Data collection was 98.1% complete to 25o.  A total of 39280 partial and complete reflections were collected covering the indices, h = -9 to 9, k = -22 to 23, l = -29 to 30.  6770 reflections were symmetry independent and the Rint = 0.0466 indicated that the data was above average quality (0.07). 

Indexing and unit cell refinement indicated a orthorhombic lattice.  The space group was found to be P 21/c (No. 14). 

The data was integrated and scaled using hkl-SCALEPACK. This program applies a multiplicative correction factor (S) to the observed intensities (I) and has the following form:


[image: image1.wmf]22

2(sin)/

S = ()/scale

B

e

ql

-


S is calculated from the scale and the B factor determined for each frame and is then applied to I to give the corrected intensity (Icorr).

Solution by direct methods (SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. 

All hydrogen atoms were located using a riding model. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares. 

While the water hydrogen atoms hydrogen bond to otf oxygen O8 and O9', O1 donates to water O3 and O5' of an otf, and O2 to O6 and O7' of neighboring otf solvents (hyphenated atoms from symmetry related molecules). 





_1097643391.unknown

