Crystal Structure Report for Heinekey
Submitted by Inigo Aguirre de Carcer 

Sample ID – S3Si2Fe
by Jason Benedict and John Freudenthal
X-ray Crystallography Laboratory

University of Washington

28. August 2006
Data backup accessibly through http:

URL: 
http://cad4.cpac.washington.edu/structures/heineke/inigo/S3Si2Fe
Username: 
xray-user

Password: 
hkl-data

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210 

Email: kaminsky@wintensor.com
Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures. Even I  have to pay for my own structures for my research.

A red crystal block cut down to 0.1 x 0.1 x 0.1 mm was mounted on a glass capillary with oil.  Data was collected at -143oC with one set of exposure as follows:

Scan 

Type
Scanlength (deg.)  start (deg.)
(     
(
(     
( 

1
      
(        
172.0




3.70
39.5
160  
 0
2

(
91.5




3.70
94
-200
74

3

(
41.5




3.7
-145
-170
74      

Crystal-to-detector distance was 30 mm and exposure time was 30 seconds per degree for all sets.  The scan width was 2.0o.   Data collection was 99.8% complete to 25.00o in (.  A total of 38806 partial and complete reflections were collected covering the indices, h = -32 to 32, k = -15 to 15,  l = -21 to 21.  5101 reflections were symmetry independent and the Rint = 0.0607 indicated that the data was of slightly better than average quality (0.07). 

Indexing and unit cell refinement indicated a monoclinic C lattice.  The space group was found to be C 2/c (No.15). 

The data was integrated and scaled using hkl-SCALEPACK. This program applies a multiplicative correction factor (S) to the observed intensities (I) and has the following form:

S = exp(2B(sinq/()2)/ scale

S is calculated from the scale and the B factor is determined for each frame and is then applied to I to give the corrected intensity (Icorr).

Solution by direct methods (SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. 

All hydrogen atoms were located using a riding model. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares. 

The sample solved in the space group C 2/c with an asymmetrical unit as shown with protons excluded for clarity.  The asymmetric unit consists of an iron bound to three sulfur atoms and two carbon monoxide ligands.  The full molecule, generated via a center of inversion from the asymmetric unit, is depicted on the following page.  Also included is a projection of the molecule including proton.



