Crystal Structure Report for 
Prof. Karen Goldberg
Submitted by Susan Kloek
Sample ID – SMK001
by Antonio DiPasquale
X-ray Crystallography Laboratory

University of Washington

23. April 2004
Data backup accessibly through ftp:

computer: 

chmraypc.cpac.washington.edu

login: 

anonymous

password:

(your name or email address)

location: 
c:\structures\goldberg\kloek\SMK001
Data backup accessibly through http:

URL: 
http://cad4.cpac.washington.edu/structures
Username: 
xray-user

Password: 
hkl-data

A.DiPasquale:(206) 616-4212

(x-ray lab):     (206) 543-0210 

Email:
adipasqu@u.washington.edu
Understanding crystallographic information is not trivial, if you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.  For many structures, it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures. Even we have to pay for our own structures for our research.

An orange crystal prism 0.10 × 0.04 × 0.04 mm in size was mounted on a glass capillary with oil.  Data was collected at -143oC with three sets of exposures as follows:

Scan 

Type
Scanlength (deg.)  start (deg.):(     
      (
         (     
 ( 

1
      
(        
181.6


          
 3.703   -52.297   160.000     0.000      

2

ω
91.5



 3.703   -25.904  -200.073   74.141
3

ω         41.5



 3.703
  94.096  -180.073   74.141

Crystal-to-detector distance was 30 mm and exposure time was 20 seconds per degree for all sets.  The scan width was 2.0o.   Data collection was 99.9% complete to 25o in (.  A total of 33,027 partial and complete reflections were collected covering the indices, h = -21 to 21, k = -14 to 14,

 l = -22 to 22.  7,467 reflections were symmetry independent and the Rint = 0.0961 indicated that the data was of slightly less than average quality (0.07). 

Indexing and unit cell refinement indicated a monoclinic P lattice.  The space group was found to be P 21/c (No.14). 

The data was integrated and scaled using hkl-2000. This program applies a multiplicative correction factor (S) to the observed intensities (I) and has the following form:


[image: image1.wmf]22

2(sin)/

S = ()/scale

B

e

ql

-


S is calculated from the scale and the B factor, which is determined for each frame and is then applied to I to give the corrected intensity (Icorr).

Solution by direct methods (SIR-97) produced a complete heavy atom phasing model consistent with the proposed structure. 

All hydrogen atoms were placed using a riding model. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares (SHELXL-97).



_1097643391.unknown

