Crystal Structure Report for Robinson

Submitted by Yi Liao

Sample ID – YL074

by Jason B. Benedict

and Werner Kaminsky

X-ray Crystallography Laboratory

University of Washington

20. May 2003
Data backup accessibly through ftp:

computer: 

chmraypc.cpac.washington.edu

login: 

anonymous

password:

(your name or email address)

location: 
c:\structures\robinson\yi\YL074

Data backup accessibly through http:

URL: 
http://cad4.cpac.washington.edu/structures
Username: 
xray-user

Password: 
hkl-data

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210 

Email: kaminsky@wintensor.com
Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures. Even I  have to pay for my own structures for my research.

A green crystal prism 0.24 x 0.24 x 0.12 mm was mounted on a glass capillary with oil.  Data was collected at -143oC with one set of exposure as follows:

Scan 

Type
Scanlength (deg.)  start (deg.)
(     
(
(     
( 

1
      
(        
182.0




3.70
39.5
160  
 0      

Crystal-to-detector distance was 30 mm and exposure time was 30 seconds per degree for all sets.  The scan width was 2.0o.   Data collection was 95.8% complete to 24.70o in (.  A total of 30257 partial and complete reflections were collected covering the indices, h = -32 to 32, k = -17 to 16,  l = -22 to 22.  5029 reflections were symmetry independent and the Rint = 0.0737 indicated that the data was of slightly less than average quality (0.07). 

Indexing and unit cell refinement indicated a monoclinic C lattice.  The space group was found to be C2/c (No.15). 

The data was integrated and scaled using hkl-SCALEPACK. This program applies a multiplicative correction factor (S) to the observed intensities (I) and has the following form:

S = exp(2B(sinq/()2)/ scale

S is calculated from the scale and the B factor is determined for each frame and is then applied to I to give the corrected intensity (Icorr).

Solution by direct methods (SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. 

All hydrogen atoms were located using a riding model. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares. 

[image: image1.wmf]C34

Cl1

Cl2

C16

C15

C14

C13

S1

C12

C11

C1

Fe1

C4

C3

C2

C8

C9

C10

C6

C28

C29

C24

C23

F3

F2

F1

C22

O1

C21

C31

C32

N2

C33

N3

C20

C30

N1





