Crystal Structure Report for Robinson

Submitted by Yi Liao 

Sample ID – YLII100

by Jason B. Benedict  

and Werner Kaminsky

X-ray Crystallography Laboratory

University of Washington

25. October 2004
Data backup accessibly through ftp:

computer: 

chmraypc.cpac.washington.edu

login: 

anonymous

password:

(your name or email address)

location: 
c:\structures\robinson\yi\YLII100

Data backup accessibly through http:

URL: 
http://cad4.cpac.washington.edu/structures
Username: 
xray-user

Password: 
hkl-data

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210 

Email: kaminsky@wintensor.com
Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures. Even I  have to pay for my own structures for my research.

A dark red crystal prism cut down to 0.19 x 0.24 x 0.26 mm was mounted on a glass capillary with oil.  Data was collected at -143oC with two sets of exposure as follows:

Scan 

Type
Scanlength (deg.)  start (deg.)
(     
(
(     
( 

1
      
(        
183.0




3.70
-1.5
160  
 0 

2
      
(        
61.5




3.70
94.1
-200.1 
 74.1     
2
      
(        
21.5




3.70
-25.9
-160 
 74.1        

Crystal-to-detector distance was 30 mm and exposure time was 20 seconds per degree for all sets.  The scan width was 1.5o.   Data collection was 90.6% complete to 26.37o and 94.3% complete to 25o  in (.  A total of 16071 partial and complete reflections were collected covering the indices, h = -11 to 10, k = -11 to 10,  l = -13 to 15. 3783 reflections were symmetry independent and the Rint = 0.0853 indicated that the data was of slightly less than average quality (0.07). 

Indexing and unit cell refinement indicated a triclinic P lattice.  The space group was found to be P(1 (No.2). 

The data was integrated and scaled using hkl-SCALEPACK. This program applies a multiplicative correction factor (S) to the observed intensities (I) and has the following form:

S = exp(2B(sinq/()2)/ scale

S is calculated from the scale and the B factor is determined for each frame and is then applied to I to give the corrected intensity (Icorr).

Solution by direct methods (SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. 

All hydrogen atoms were located using a riding model. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares. 

The crystals pack as hydrogen bonded centro-symmetric head to tail dimers with overlap in the acceptor end of the NLO chromophore. Details of the hydrogen bonding between O1 and N3 are included in the shelxl.tex report. Further more the molecules exhibit substantial bowing along the long axis of the molecule and there is significant twisting of the molecule about the C4-C7 bond. While the molecule is chiral, the structure is centro-symmetric and thus contains an equal amount of both enantiomers.




