Crystal Structure Report for Michael

Submitted by Brian Cochran 

Sample ID – BMC-F-43-1

by Jason Benedict and Erica Gunn

X-ray Crystallography Laboratory

University of Washington

09. February 2006
Data backup accessibly through http:

URL: 
http://cad4.cpac.washington.edu/structures
Username: 
xray-user

Password: 
hkl-data

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210 

Email: kaminsky@wintensor.com
Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures. Even I  have to pay for my own structures for my research.

A clear crystal plate cut down to 0.24 x 0.12 x 0.05 mm was mounted on a glass capillary with oil.  Data was collected at -143oC with two sets of exposure as follows:

Scan 

Type
Scanlength (deg.)  start (deg.)
(     
(
(     
( 

1
      
(        
173.4




7.80
-152.2
160  
 0 

2
      
(         86.8




7.80
94.09
-201.8 
 74.1           

Crystal-to-detector distance was 40 mm and exposure time was 75 seconds per degree for all sets.  The scan width was 1o.   Data collection was 99.2% complete to 26.37o and 99.7% complete to 25o  in (.  A total of  61090 partial and complete reflections were collected covering the indices, h = -13 to 13, k = -15 to 15,  l = -40 to 40.  8786 reflections were symmetry independent and the Rint = 0.156 indicated that the data was of less than average quality (0.07). 

Indexing and unit cell refinement indicated a orthorhombic P lattice.  The space group was found to be P212121 (No.19). 

The data was integrated and scaled using hkl-SCALEPACK. This program applies a multiplicative correction factor (S) to the observed intensities (I) and has the following form:


[image: image1.wmf]22

2(sin)/

S = ()/scale

B

e

ql

-


S is calculated from the scale and the B factor determined for each frame and is then applied to I to give the corrected intensity (Icorr).

Solution by direct methods (SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. 

All hydrogen atoms were located using a riding model. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares. 

Several bond lengths in the pentane solvent molecule needed to be restrained due to excessive motion within the lattice. Crystal decomposition supports the assignment of this volatile solvent within the lattice. The space group was found to be chiral, P212121. Refinement correcting for the inverse twin revealed that the lattice contained 58% of the asymmetric unit as shown and 42% of the inverse twin.  



_1097643391.unknown

