Crystal Structure Report for Kovacs

Submitted by Lisa Brines

Sample ID – Brines13

by Jason Benedict 

and Werner Kaminsky

X-ray Crystallography Laboratory

University of Washington

09. August 2006
Data backup accessibly through http:

URL: 
http://cad4.cpac.washington.edu/structures/kovacs/brines/brines13

Username: 
xray-user

Password: 
hkl-data

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210 

Email: kaminsky@wintensor.com
Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures. Even I  have to pay for my own structures for my research.

A purple crystal plate 0.48 x 0.36 x 0.07 mm was mounted on a glass capillary with oil.  Data was collected at -143oC with two sets of exposure as follows:

Scan 

Type
Scanlength (deg.)  start (deg.)
(     
(
(     
( 

1
      
(        
168.1




8.972
-99.03
160  
 0 

2
      
(        
48.6




8.972
145.9
-185 
 -74.1           

Crystal-to-detector distance was 43.5 mm and exposure time was 60 seconds per degree for all sets.  The scan width was 1o.   Data collection was 99.0% complete to 25.68o and 99.0% complete to 25o  in (.  A total of 74378 partial and complete reflections were collected covering the indices, h = -15 to 15, k = -20 to 20, l = -44 to 44. 7279 reflections were symmetry independent and the Rint = 0.0971 indicated that the data was of less than average quality (0.07). 

Indexing and unit cell refinement indicated an orthorhombic P lattice.  The space group was found to be P b c a (No.61). 

The data was integrated and scaled using hkl-SCALEPACK. This program applies a multiplicative correction factor (S) to the observed intensities (I) and has the following form:


[image: image1.wmf]22

2(sin)/

S = ()/scale

B

e

ql

-


S is calculated from the scale and the B factor determined for each frame and is then applied to I to give the corrected intensity (Icorr).

Solution by direct methods (SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. 

All hydrogen atoms were located using a riding model. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares. 

The asymmetric unit of this structure consists of an oxo-bridged Mn dimer, two PF6 anions (one of which was disordered about an F-P-F axis) and one acetonitrile solvent molecule. Additional disorder was observed on carbon 6 which was split into two positions shown in orange and blue on the following page. The occupancy of C6a was 61% and 39% for C6b. The crystals were of rather poor quality, most likely due to decomposition arising from solvent loss. 




_1097643391.unknown

