Crystal Structure Report for Kovacs
Submitted by Lisa Brines 

Sample ID – BRINES15
by John Freudenthal
and Werner Kaminsky
X-ray Crystallography Laboratory

University of Washington

17. October 2006
Data backup accessibly through http:

URL: 
http://cad4.cpac.washington.edu/structures/
Username: 
xray-user

Password: 
hkl-data

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210 

Email: kaminsky@wintensor.com
Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures. Even I  have to pay for my own structures for my research.

A clear yellow crystal plate cut down to 0.5 x 0.4 x 0.2 mm was mounted on a glass capillary with oil.  Data was collected at -143oC with four sets of exposure as follows:

Scan 

Type
Scanlength (deg.)  start (deg.)
(     
(
(     
( 

1
      
(        
181.0




3.70
-109
160  
0
2

(
41.5




3.70
-26
-190
74      

3

(
86.5




3.70
-26
-200
74      

4

(
28




3.70
26
-174
-74      
Crystal-to-detector distance was 30 mm and exposure time was 40 seconds per degree for all sets.  The scan width was 1.0o.   Data collection was 97.5% complete to 28.32 o in ( and 97.5% to 25.0o in (.  A total of  68872 partial and complete reflections were collected covering the indices, h = -20 to 20, k = -12 to 12,  l = -24 to 23.  5866 reflections were symmetry independent and the Rint = 0.0421 indicated that the data was of better than average quality (0.07). 

Indexing and unit cell refinement indicated a monoclinic P lattice.  The space group was found to be P2/c (No.13). 

The data was integrated and scaled using hkl-SCALEPACK. This program applies a multiplicative correction factor (S) to the observed intensities (I) and has the following form:


[image: image1.wmf]22

2(sin)/

S = ()/scale

B

e

ql

-


S is calculated from the scale and the B factor is determined for each frame and is then applied to I to give the corrected intensity (Icorr).

Solution by direct methods (SHELXS) produced a complete heavy atom phasing model consistent with the proposed structure. 

All hydrogen atoms were located using a riding model. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares. 

The molecule appears to be a dimer with each half being related by a twofold symmetry with the rotation axis passing through Fe2.  The dimer consists of three iron atoms. The dimer is positively charged where two chlorides (the two-fold- symmetry related one to Cl1 is not shown) counterbalance that charge.  A methylene dichloride solvent (disordered) and a disordered water complete the structure.



_1097643391.unknown

