Crystal Structure Report for 
Sei-Hum Jang
by Werner Kaminsky

Sample Submitted by Francis Lin
ID – Cranfis_17_2
X-ray Crystallography Laboratory

University of Washington

12. February 2021
Data Collection  started: 2/8/2021
Documentation finished: 2/12/2021
Data backup accessibly through http:

URL: http://cad4.cpac.washington.edu/structures
W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210 

Email: kaminsky@chem.washington.edu
Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures. 

A black prism, measuring 0.30 x 0.20 x 0.05 mm3 was mounted on a loop with oil.  Data was collected at -173oC on a Bruker APEX II single crystal X-ray diffractometer, Mo-radiation.
Crystal-to-detector distance was 40 mm and exposure time was 180 seconds per frame for all sets.  The scan width was 0.5o.   Data collection was 100% complete to 24.257o  in (.  A total of  56351 unique reflections were collected covering the indices, -15<=h<=15, -26<=k<=26, -36<=l<=36,   Rint = 0.2969 (of twinned data). Indexing and unit cell refinement indicated a triclinic lattice.  The space group was found to be P(1  (No. 2). 

The data was integrated and scaled using SAINT, SADABS within the APEX2 software package by Bruker.
 

The data appeared twinned via 180 degrees about (0 0 1) and a HKLF 5 file was created two allow twin refinement in SHELXL.
The contribution of disordered solvent to the diffraction pattern was removed with SQUEEZE

Solution by direct methods (SHELXS, SIR97
) did not produce a complete heavy atom phasing model. The structure was completed by difference Fourier synthesis with SHELXL97.
,
 Scattering factors are from Waasmair and Kirfel
. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C---H distances in the range 0.95-1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares.
The structure is of sufficient quality suitable for publication. Table 1 summarizes the data collection details. Figure 1 shows an ORTEP
 of the asymmetric unit.
[image: image1.jpg]



Figure 1. ORTEP of the structure with thermal ellipsoids at the 50% probability level. Disorder and SQUEEZEd solvent omitted for clarity.

Table 1: Crystallographic data for the structures provided.

Empirical formula 
C86 H94 F4 N8 O2 S3 Se2

Formula weight 
1601.79

Temperature 
100(2) K

Wavelength 
0.71073 Å

Crystal system 
Triclinic

Space group 
P -1

Unit cell dimensions
a = 13.6074(16) Å
= 70.140(9)°.


b = 23.215(3) Å
= 84.235(8)°.


c = 31.455(4) Å
 = 82.491(9)°.

Volume
9249(2) Å3
Z
4

Density (calculated)
1.150 Mg/m3
Absorption coefficient
0.921 mm-1
F(000)
3336

Crystal size
0.300 x 0.200 x 0.050 mm3
Theta range for data collection
1.335 to 24.257°.

Index ranges
-15<=h<=15, -26<=k<=26, -36<=l<=36

Reflections collected
56351

Independent reflections
56351 [R(int) = 0.2969]

Completeness to theta = 24.257°
100.0 % 

Refinement method
Full-matrix least-squares on F2
Data / restraints / parameters
56351 / 3766 / 2072

Goodness-of-fit on F2
1.077

Final R indices [I>2sigma(I)]
R1 = 0.1670, wR2 = 0.3521

R indices (all data)
R1 = 0.4291, wR2 = 0.4493

Largest diff. peak and hole
0.889 and -0.630 e.Å-3
� Bruker (2007) APEX2 (Version 2.1-4), SAINT (version 7.34A), SADABS (version 2007/4), BrukerAXS Inc, Madison, Wisconsin, USA.


� (a) A. Spek, J. Appl. Cryst. (2003), 36, 7-13; 


   (b) P. van der Sluis & A. L. Spek, Acta Cryst. (1990). A46, 194-201.


   (c) Spek, A. L. (2009). Acta. Cryst. D65, 148-155.


� (a) Altomare A, Burla C, Camalli M, Cascarano G L, Giacovazzo C, Guagliardi A,   Moliterni AGG, Polidori G, Spagna R. (1999) SIR97: a new tool for crystal structure determination and refinement Journal of Applied Crystallography, 32, 115-119. 


   (b) Altomare A, Cascarano G L, Giacovazzo C, Guagliardi A. (1993) Completion and refinement of crystal structures with SIR 92. Journal of Applied Crystallography, 26, 343-350.


� (a) Sheldrick GM. (1997) SHELXL-97, Program for the Refinement of Crystal Structures. University of Göttingen, Germany.


   (b) Sheldrick GM. (2013) Crystal structure refinement with SHELXL. Acta Cryst. (2015). C71, 3-8.


� Mackay, S.; Edwards, C.; Henderson, A.; Gilmore, C.; Stewart, N.; Shankland, K.; Donald, A. (1997) MaXus: a computer program for the solution and refinement of crystal structures from diffraction data. University of Glasgow, Scotland,.


� Waasmaier, D.; Kirfel, A. (1995) New Analytical Scattering Factor Functions for Free Atoms and Ions. Acta Crystallographica A., 51, 416-430.


� Farrugia LJ. (1997) Ortep-3 for Windows. Journal of Applied Crystallography, 30, 565





