Crystal Structure Report for Julie Kovacs
by M. Coggins and W. Kaminsky
Sample Submitted by M. Coggins 

ID – michael036
X-ray Crystallography Laboratory

University of Washington

04. April 2011
Data backup accessibly through http:

URL: 
http://cad4.cpac.washington.edu/structures
Username: 
xray-user

Password: 
hkl-data

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210 

Email: kaminsky@chem.washington.edu
Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures. Even I  have to pay for my own structures for my research.

A colorless plate, measuring 0.20 x 0.20 x 0.15 mm3 was mounted on a glass capillary with oil.  Data was collected at -173oC on a Bruker APEX II single crystal X-ray diffractometer, Mo-radiation.
Crystal-to-detector distance was 40 mm and exposure time was 10 seconds per degree for all sets.  The scan width was 0.5o.   Data collection was 99.4% complete to 25o  in (.  A total of  63341 (merged) reflections were collected covering the indices, h = -13 to 13, k = -17 to 17,  l = -18 to 18.  8954 reflections were symmetry independent and the Rint = 0.0519 indicated that the data was good (average quality 0.07).  Indexing and unit cell refinement indicated a triclinic lattice.  The space group was found to be P(1  (No.2). 

The data was integrated and scaled using SAINT, SADABS within the APEX2 software package by Bruker.
 

Solution by direct methods (SHELXS, SIR97
) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL97.
,
 Scattering factors are from Waasmair and Kirfel
. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C---H distances in the range 0.95-1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares.
The structure is of high quality and ready for publication. Table 1 summarizes the data collection details. Figure 1 shows an ORTEP
 of the asymmetric unit.
[image: image1.png]59 Y

s41 2011 - (240311

4 22:06

PLATON-Apr-

N
—
N
[@)]

1

N1

C1g

ci8

NOMOVE FORCED

RES=

Prob
Temp

0

noau
—
Oul
oo

-42 X





Figure 1. ORTEP of the structure with thermal ellipsoids at the 50% probability level. 
Table 1: Crystallographic data for the structures provided.

Empirical formula 
C43 H48 B N5

Formula weight 
645.67

Temperature 
100(2) K

Wavelength 
0.71073 Å

Crystal system 
Triclinic

Space group 
P -1

Unit cell dimensions
a = 10.1598(6) Å
= 80.551(3)°.


b = 13.2629(9) Å
= 81.648(3)°.


c = 13.7476(9) Å
 = 85.125(3)°.

Volume
1804.4(2) Å3
Z
2

Density (calculated)
1.188 Mg/m3
Absorption coefficient
0.070 mm-1
F(000)
692

Crystal size
0.20 x 0.20 x 0.15 mm3
Theta range for data collection
1.52 to 28.44°.

Index ranges
-13<=h<=13, -17<=k<=17, -18<=l<=18

Reflections collected
63341

Independent reflections
8954 [R(int) = 0.0519]

Completeness to theta = 25.00°
99.4 % 

Max. and min. transmission
0.9896 and 0.9862

Refinement method
Full-matrix least-squares on F2
Data / restraints / parameters
8954 / 0 / 446

Goodness-of-fit on F2
1.017

Final R indices [I>2sigma(I)]
R1 = 0.0466, wR2 = 0.0958

R indices (all data)
R1 = 0.0859, wR2 = 0.1119

Largest diff. peak and hole
0.268 and -0.235 e.Å-3



� Bruker (2007) APEX2 (Version 2.1-4), SAINT (version 7.34A), SADABS


(version 2007/4), BrukerAXS Inc, Madison, Wisconsin, USA.


� (a) Altomare, A.; Burla, C.; Camalli M.; Cascarano L.; Giacovazzo C.; Guagliardi A.;   Moliterni A.G.G.; Polidori G.; Spagna R. J. Appl. Cryst. 1999, 32, 115-119; (b) Altomare, A., Cascarano, G., Giacovazzo, C., Guagliardi, A., J. Appl. Cryst. 1993, 26, 343.


� Sheldrick, G. M. SHELXL-97: Program for the Refinement of Crystal Structures 1997 University of Gottingen, Germany.


� Mackay, S.; Edwards, C.; Henderson, A.; Gilmore, C.; Stewart, N.; Shankland, K.; Donald, A.; MaXus: a computer program for the solution and refinement of crystal structures from diffraction data. University of Glasgow, Scotland, 1997.


� Waasmaier, D.; Kirfel, A. Acta Crystallogr. A. 1995, 51, 416.


� Farrugia, L. J. Appl. Cryst. 1997, 30, 565





