Crystal Structure Report for Kovacs

Submitted by Santiago Toledo 

Sample ID – Santiago14

by John Freudenthal & W.K.

X-ray Crystallography Laboratory

University of Washington

07. July 2008
Data backup accessibly through http:

URL: 
http://cad4.cpac.washington.edu/structures/kovacs/santiago/santiogo14

Username: 
xray-user

Password: 
hkl-data

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210 

Email: kaminsky@wintensor.com
Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures. Even I  have to pay for my own structures for my research.

A green crystal of 0.1 x 0.08 x 0.08 mm was mounted on a glass capillary with oil.  Data was collected at -143oC with one set of exposure as follows:

Scan 

Type
Scanlength (deg.)  start (deg.)
(     
(
(     
( 

1
      
(        
182




3.70
-160
160  
0

2
      
(        
92




3.70
-94
-200  
74

3
      
(        
20




3.70
146
-165  
-74

Crystal-to-detector distance was 30 mm and exposure time was 15 seconds per degree for all sets.  The scan width was 2.0o.   Data collection was 95.6% complete to 25.0o in (.  A total of 100301 partial and complete reflections were collected covering the indices, h = -14 to 14, k = -35 to 35,  l = -19 to 19.  10542 reflections were symmetry independent and the Rint = 0.06 indicated that the data was of better than quality (0.07). 

Indexing and unit cell refinement indicated an orthorhombic P lattice.  The space group was found to be P 21/a (No. 14).

The data was integrated and scaled using hkl-SCALEPACK. This program applies a multiplicative correction factor (S) to the observed intensities (I) and has the following form:

S = exp(2B(sinq/()2)/ scale

S is calculated from the scale and the B factor is determined for each frame and is then applied to I to give the corrected intensity (Icorr).

Solution by direct methods (SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. 

All hydrogen atoms were located using a riding model. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares. 




