Crystal Structure Report for M Heinekey
by W. Kaminsky and M. Coggins
Sample by Skye Rios & Joe Meredith 

ID – ser0135
X-ray Crystallography Laboratory

University of Washington

16. August 2010
Data backup accessibly through http:

URL: 
http://cad4.cpac.washington.edu/structures
Username: 
xray-user

Password: 
hkl-data

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210 

Email: kaminsky@chem.washington.edu
Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures. Even I  have to pay for my own structures for my research.

An orange prism, measuring 0.04 x 0.05 x 0.08 mm3 was mounted on a glass capillary with oil. 
The sample batch contained also red crystals that turned out to be some sort of starting material co-crystallized with an unidentified additional compound, resembling AgCl or similar. Data was collected at -173oC on a Bruker APEX II single crystal X-ray diffractometer, Mo-radiation.
Crystal-to-detector distance was 40 mm and exposure time was 30 seconds per degree for all sets.  The scan width was 0.5o.  The raw data appeared twinned although the sample looked homogeneous. With cell now
 a 138.7 degrees twin rotation about (-0.006 0.248 1) was found which, if unresolved, caused considerable overlap of diffraction peak intensities from different domains of the sample. Multi-domain integration with SAINT within the APEX2 software package by Bruker
 and absorption correction with twinabs
 removed the overlap. Data collection was 97.5% complete to 25o  in (.  A total of 2472 independent reflections were collected covering the indices, h = 0 to 18, k = 0 to 11,  l = -21 to 0. The Rint = 0.0292 indicated that the data was excellent (average quality 0.07).  Indexing and unit cell refinement indicated a primitive non-centrosymmetric orthorhombic lattice.  The space group was found to be P n a 21  (No.33). 

Solution by direct methods (SHELXS, SIR97
) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL97.
,
 Scattering factors are from Waasmair and Kirfel
. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C---H distances in the range 0.95-1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares.
Thermal parameters of a few of the tp* atoms needed stabilizing measures to insure refinement convergence despite the good statistical parameters. The crystals are enantiomorphically twinned (racemate) in addition to the rotational twin.
The structure is of high quality and ready for publication. Table 1 summarizes the data collection details. Figure 1 shows an ORTEP
 of the asymmetric unit.

<ser0135.jpg>
Figure 1. ORTEP of the structure with thermal ellipsoids at the 50% probability level. 
<ser0135_photo.jpg>
Figure 2. Crrystal phot
Table 1: Crystallographic data for the structures provided.

Identification code 
twin4a

Empirical formula 
C19 H25 Cl2 Ir N2

Formula weight 
544.51

Temperature 
100(2) K

Wavelength 
0.71073 Å

Crystal system 
Orthorhombic

Space group 
P n a 21

Unit cell dimensions
a = 13.6170(5) Å
= 90°.


b = 8.7826(3) Å
= 90°.


c = 16.3065(5) Å
 = 90°.

Volume
1950.14(11) Å3
Z
4

Density (calculated)
1.855 Mg/m3
Absorption coefficient
7.123 mm-1
F(000)
1056

Crystal size
0.08 x 0.05 x 0.04 mm3
Theta range for data collection
2.50 to 28.43°.

Index ranges
0<=h<=18, 0<=k<=11, -21<=l<=0

Reflections collected
2472

Independent reflections
2472 [R(int) = 0.0292]

Completeness to theta = 25.00°
97.5 % 

Max. and min. transmission
0.7637 and 0.5996

Refinement method
Full-matrix least-squares on F2
Data / restraints / parameters
2472 / 43 / 225

Goodness-of-fit on F2
1.074

Final R indices [I>2sigma(I)]
R1 = 0.0395, wR2 = 0.0755

R indices (all data)
R1 = 0.0473, wR2 = 0.0781

Absolute structure parameter
0.45(4)

Largest diff. peak and hole
2.603 and -1.371 e.Å-3



� Sheldrick, G. M. (2005). CELL_NOW. University of Goettingen, Germany.


� Bruker (2007) APEX2 (Version 2.1-4), SAINT (version 7.34A), SADABS


(version 2007/4), BrukerAXS Inc, Madison, Wisconsin, USA.


� Sheldrick, G. M. (2007). TWINABS. University of Goettingen, Germany.


� (a) Altomare, A.; Burla, C.; Camalli M.; Cascarano L.; Giacovazzo C.; Guagliardi A.;   Moliterni A.G.G.; Polidori G.; Spagna R. J. Appl. Cryst. 1999, 32, 115-119; (b) Altomare, A., Cascarano, G., Giacovazzo, C., Guagliardi, A., J. Appl. Cryst. 1993, 26, 343.


� Sheldrick, G. M. SHELXL-97: Program for the Refinement of Crystal Structures 1997 University of Gottingen, Germany.


� Mackay, S.; Edwards, C.; Henderson, A.; Gilmore, C.; Stewart, N.; Shankland, K.; Donald, A.; MaXus: a computer program for the solution and refinement of crystal structures from diffraction data. University of Glasgow, Scotland, 1997.


� Waasmaier, D.; Kirfel, A. Acta Crystallogr. A. 1995, 51, 416.


� Farrugia, L. J. Appl. Cryst. 1997, 30, 565





