Crystal Structure Report for 
Prof. Jim Mayer
Submitted by Todd Markle
Sample ID – tfm1-179
by Antonio DiPasquale (corrected by W. Kaminsky)
X-ray Crystallography Laboratory

University of Washington

18. March 2005
Data backup accessibly through ftp:

computer: 

chmraypc.cpac.washington.edu

login: 

anonymous

password:

(your name or email address)

location: 
c:\structures\mayer\markle\tfm1-179
Data backup accessibly through http:

URL: 
http://cad4.cpac.washington.edu/structures
Username: 
xray-user

Password: 
hkl-data

A.DiPasquale:(206) 616-4212

(x-ray lab):     (206) 543-0210 

Email:
adipasqu@u.washington.edu
A colorless prism was cut to 0.24 × 0.24 × 0.12 mm in size was mounted on a glass capillary with oil.  Data was collected at -143oC with three sets of exposures as follows:

Scan 

Type
Scanlength (deg.)  start (deg.):(     
      (
         (     
 ( 

1
      
(        
182.0


          
3.703  -176.500   160.000     0.000      

2

ω
81.5



3.703  -145.904  -195.073   74.141
3

ω         31.5



3.703
 -25.904  -170.073   74.141

Crystal-to-detector distance was 30 mm and exposure time was 15 seconds per degree for all sets.  The scan width was 2.0o.   Data collection was 96.7% complete to 25o in (.  A total of 15,217 partial and complete reflections were collected covering the indices, h = -40 to 40, k = -16 to 17,

 l = -10 to 10.  3,972 reflections were symmetry independent and the Rint = 0.0690 indicated that the data was of average quality (0.07). 

Indexing and unit cell refinement indicated a monoclinic C lattice.  The space group was found to be C 2/c (No.15). 

The data was integrated and scaled using hkl-2000. This program applies a multiplicative correction factor (S) to the observed intensities (I) and has the following form:


[image: image1.wmf]22

2(sin)/

S = ()/scale

B

e

ql

-


S is calculated from the scale and the B factor, which is determined for each frame and is then applied to I to give the corrected intensity (Icorr).

Solution by direct methods (SIR-97) produced a complete heavy atom phasing model consistent with the proposed structure. 

All hydrogen atomswere placed using a riding model. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares (SHELXL-97).  If the hydroxyl protons, H1 and H2 were located from the difference map and their positions were refined isotropically, the distance of H1 to O1 was encreased significantly indicating strong hydrogen bonding to O2. However, a O-H bond of 1.2Angstrom will be rejected by the IUCr. H1 and H2 thus were included with constrained bond distances.
Models of the unit cell packing clearly show a hydrogen bonding network between H2 and N1 in an adjacent molecule (see Table 7).




_1097643391.unknown

